## Slide 1
GB as Dislocation structure/ Frank-Bilby Analysis
A. Sutton and R. Balluffi (1996), Interfaces in Crystalline Materials, Oxford
b burgers vector
<110> and <100> type
ξ ρ
Line direction
Misorientation axis
w dislocation density
B Net Burgers
Notes: General boundaries require 3 sets of Burgers vectors.
Certain symmetric tilts can be constructed with only 1 Burgers vector (112, 100 axes in fcc with <110> Burgers vectors).
we need <100> dislocations in order to match the Cahn-Mishin simulations
Less symmetric tilts require 2 Burgers vectors.
Twist boundaries require at least 2 Burgers vectors.
First we find the sets of 3 indepent burgers
And calculate the reciprocal burgers vector set
Vectors in the GB plane normal to the line directions