## Slide 1: 27-750, Advanced Characterization and Microstructural Analysis: Texture and its Effect on Anisotropic Properties
Tony (A.D.) Rollett, Carnegie Mellon Univ.
Last revised: 12th Jan. 2014

## Slide 2: Microstructure-Properties Relationships
Microstructure
Properties
Processing
Performance
Design

## Slide 3: Course Objective
Many courses deal with microstructure-properties relationships, so what is special about this course?!
Despite the crystalline nature of most useful and interesting materials, crystal alignment and the associated anisotropy is ignored. Yet, most properties are sensitive to anisotropy. Therefore microstructure should include crystallographic orientation (“texture”).
The objective of this course is to provide you with the tools to understand and quantify various kinds of texture and to solve problems that involve texture and anisotropy.

## Slide 4: Questions
Examples of questions that you should be able to answer with the knowledge and skills provided by this course:
What is a “fiber texture”?
Why is a <111>//ND texture ideal for deep drawing?
Why is obtaining a <111> fiber texture difficult in FCC metals, but straightforward in BCC?
Why are intensity values generally much higher in the Orientation Distribution than in the corresponding pole figures?
How is it possible to recover the full 5-parameter distribution of grain boundary character from a plane section and yet one can only measure 4 out of 5 parameters for an individual boundary in that plane section?
What do the units “Multiples of a Random/Uniform Distribution” mean? Why are distributions scaled differently in texture than in statistics?
Why was solving the problem of calculating an orientation distribution from pole figures a fundamental advance in texture analysis? Hint: think about the parameterization of rotations.
Why do we need 3 (and only 3) parameters to describe a rotation?
How do Miller indices, orthogonal matrices, Rodrigues parameters and quaternions relate to each other?
What is epitaxy? What is apotaxy (not apoplexy!)?
Why do textures develop during plastic deformation?

## Slide 5: Encyclopedia Britannica, texture
  Texture refers to the physical makeup of rock--namely, the size, shape, and arrangement (packing and orientation) of the discrete grains or particles of a sedimentary rock. Two main natural textural groupings exist for sedimentary rocks: clastic (or fragmental) and nonclastic (essentially crystalline). Noncarbonate chemical sedimentary...

## Slide 6: Websters’ Dictionary, fabric
Main Entry: fab·ric
Pronunciation: 'fa-brik
Function: noun
Etymology: Middle French fabrique, from Latin fabrica workshop, structure
Date: 15th century
1 a : STRUCTURE, BUILDING b : underlying structure : FRAMEWORK <the fabric of society>
2 : an act of constructing : ERECTION; specifically : the construction and maintenance of a church building
3 a : structural plan or style of construction b : TEXTURE, QUALITY -- used chiefly of textiles c : the arrangement of physical components (as of soil) in relation to each
other
4 a : CLOTH 1a b : a material that resembles cloth
5 : the appearance or pattern produced by the shapes and arrangement of the crystal grains in a rock

## Slide 7: Websters’ Dictionary, anisotropy
Main Entry: an·iso·trop·ic
Pronunciation: "a-"nI-s&-'trä-pik
Function: adjective
Date: 1879: exhibiting properties with different values when measured in different directions <an anisotropic crystal>
- an·iso·trop·i·cal·ly /-pi-k(&-)lE/ adverb
- an·isot·ro·py /-(")nI-'sä-tr&-pE/ also an·isot·ro·pism /-"pi-z&m/ noun

## Slide 8: People
The development of the field is greatly indebted to Hans J. Bunge who passed away in 2006.
His textbook (translated from the German original), Texture Analysis in Materials Science, is a very useful reference and many of his suggestions are only just now being developed into useful tools

## Slide 9: Microstructure
Conventional Approach: grain structure, phase structure (qualitative, image based), emphasizes interfaces and boundaries between phases.
Quantitative (conventional): grain size, aspect ratio(s), particle size, phase connectivity.
Modern Quantitative: (probability) distributions of orientation of crystal axes (relative to a reference frame) of crystals or boundaries between crystals. Properties calculated from distributions and/or microstructures with orientation included.

## Slide 10: Microstructure with Crystal Directions
Note cleavage planes within each grain: a natural indicator of crystallographic directions in a geological material.

## Slide 11: Why study texture?
Many examples exist of materials engineered to have a specific texture in order to optimize performance (single crystal turbine blades, transformer steel, magnetic thin films…).
Control of texture achievable through control of processing but many challenges remain.

## Slide 12: Texture examples
Example 1. Transformer Steel
Example 2. Anisotropic particles (whiskers) of hydroxy-apatite (HA) in polyethylene (PE)
Example 3. Earing in Deep Drawing of Cups: see slides on forming of Beer Cans
Example 4. Anisotropy of Fatigue Properties in Aerospace Al
Example 5. Effect of Grain Boundary Character on Pb Electrodes in Lead-Acid Batteries: see slides on grain boundaries and grain boundary engineering (GBE)

## Slide 13: Example 1: Transformer Steel
1935 : Goss first published his work on high permeability silicon steels.
The most commonly used material as the soft magnetic material for transformer laminations is a highly oriented albeit polycrystalline 3%Si steel; in other words, the material is almost a single crystal.
"Goss orientation" has a <110> direction normal to the sheet and a <001> parallel to the rolling direction.
Aligns the softest magnetic direction with the direction of magnetization. Thus transformers made from the textured sheet exhibit lower electrical losses.
Processing relies on a secondary recrystallization step in which all grains in a fine, primary recrystallized structure are pinned by second phase particles while the Goss grains grow to consume the entire volume.
Not clearly understood what differences in grain boundary character at the perimeter of the growing Goss grains provides them with the ability to grow at the expense of the general population.

## Slide 14: Example 2: HA particles in PE
The figure shows (a) Spherical hydroxyapatite particles (b) Whisker hydroxyapatite particles (c) Size and frequency of the hydroxyapatite particles.
Y. Zhang, K.E. Tanner, N. Gurav, and L. Di Silvio: In vitro osteoblastic response to 30 vol% hydroxyapatite polyethylene composite. J Biomed Mater Res A. 2007 May;81(2):409-17.

## Slide 15: Eg 2, contd.: HA particles in PE
The figure shows (a) An XRD orientation comparison of whisker hydroxyapatite particles and random powder (b) An XRD orientation comparison of spherical hydroxyapatite particles and random powder [Zhang et al.]. Texture is inferred from the difference between the measured powder pattern and the pattern expected for a randomly oriented material (from the powder diffraction file). This is typical in the literature as a purely qualitative measure of texture.

## Slide 16: Texture in HA in bone: refs
X-ray Pole Figure Analysis of Apatite Crystals and Collagen Molecules in Bone - all 3 versions, N Sasaki - Calcified Tissue International, 1997 - Springer
… figure analysis of mineral nanoparticle orientation in individual trabecula of human vertebral bone - all 6 versions, D Jaschouz, O Paris, P Roschger, HS Hwang, P … - Journal of Applied Crystallography, 2003 - dx.doi.org
Crystal alignment of carbonated apatite in bone and calcified tendon: results from quantitative … - all 4 versions, HR Wenk, F Heidelbach - Bone, 1999 - Elsevier
Pole figures of the orientation of apatite in bones - all 3 versions, JP Nightingale, D Lewis - Nature, 1971 - nature.com, Pole Figures of the Orientation of Apatite in Bones. ... THE orientation of the apatite and collagen in bone was first considered in this work because of its ...
Orientation of apatite in single osteon samples as studied by pole figures, A Ascenzi, E Bonucci, P Generali, A Ripamonti, N … - Calcified Tissue International, 1979 - Springer
Bone Marrow Is a Reservoir of Repopulating Mesangial Cells during Glomerular Remodeling - all 4 versions, T Ito, A Suzuki, E Imai, M Okabe, M Hori - Journal of the American Society of Nephrology, 2001 - jasn.org
Quantitative texture analysis of small domains with synchrotron radiation X-rays, F Heidelbach, C Riekel, HR Wenk - logo, 1999 - dx.doi.org

## Slide 17: Connections
Crystals are anisotropic.
A collection of crystals (a polycrystal) is therefore anisotropic unless all possible orientations are present.
Almost any processing of a material changes and biases the crystal orientations, leading to texture development.
Anisotropy can be taken advantage of; therefore it makes sense to engineer (control, design) the texture of a material.

## Slide 18: Books, Links
Course Textbook: U.F. Kocks, C. Tomé, and H.-R. Wenk, Eds. (1998). Texture and Anisotropy, Cambridge University Press, Cambridge, UK, ISBN 0-521-79420-X. This is now available as a paperback. Relevant chapters: 1, 2, 3, 4, 5, 6, 7, 8. Note that there is more detail in each chapter than we will have time to cover.
V. Randle and O. Engler, Texture Analysis: Macrotexture, Microtexture & Orientation Mapping (2000), Gordon & Breach
B.D. Cullity,(1978) Elements of X-ray Diffraction.
H.-J. Bunge, (1982) Texture Analysis in Materials Science.
A. Morawiec, Orientations and Rotations (2003), Springer.
Recent review of Texture & Anisotropy: Wenk, H. R. and P. Van Houtte (2004). “Texture and anisotropy” Reports On Progress In Physics 67 1367-1428.
Old, but still useful overview: I.L. Dillamore and W.T. Roberts (1965) “Preferred orientation in wrought and annealed metals”, Metall. Rev., 10, 271-380.
http://aluminium.matter.org.uk/content/html/eng/default.asp?catid=100&pageid=1039432491
http://code.google.com/p/mtex/

## Slide 19: Secondary References
Nye, J. F. (1957). Physical Properties of Crystals.
Ohser, J. and F. Mücklich (2000), Statistical Analysis of Microstructures in Materials Science
Reid, C. N. (1973). Deformation Geometry for Materials Scientists
Hosford, W. (1993). The Mechanics of Crystals and Textured Polycrystals, Oxford Engineering Science Series.
Khan, A.S. & S. Huang (1995). Continuum Theory of Plasticity, Wiley.
Sutton, A. P. and R. W. Balluffi (1995). Interfaces in Crystalline Materials
Gottstein, G. and L. S. Shvindlerman (1999). Grain Boundary Migration in Metals
Howe, J.M. (2000). Interfaces in Materials
Underwood, E. E., Quantitative Stereology, (1970)
http://www.msm.cam.ac.uk/phase-trans/texture.html
http://labotex.com/

## Slide 20: Topics, Activities in Course: 1
First major topic will be a discussion of orientations and how to represent them quantitatively with Miller indices, matrices, Rodrigues vectors and quaternions.
The next major topic will be x-ray pole figures and their analysis
  Every student will obtain his/her own data set
  We will first perform a standard analysis using popLA to generate an orientation distribution; then each student will measure their own pole figures and analyze the results
  The emphasis will be on development of practical skills followed up by discussion of the underlying concepts
  The objective will be to have students be competent and comfortable with pole figure analysis
Each student will report on their analyses as their project presentation at the end of the course.

## Slide 21: Topics, Activities: 2
The next major topic will be the analysis of orientation distributions
  This will involve understanding the relationships between the different methods of describing orientations, especially Euler angles and Miller indices
  We will explore the mathematical aspects of orientation space and the impact of crystal symmetry and sample symmetry
  The objective will be to develop students’ quantitative skills with orientation information so that they understand the physical meaning of orientation and texture

## Slide 22: Topics, Activities: 3
The next major topic will be to investigate orientation imaging microscopy (OIM) based on automated indexing of electron back scatter diffraction (EBSD) patterns in the scanning electron microscope (SEM)
  As with x-ray pole figures, students will first analyze a standard data set and then will make their own scan (if they are not already using EBSD) for further analysis
  The objective will be to understand the differences between sampling discrete orientations in a limited area (EBSD) and measurement of the average orientation (distribution) over a large area

## Slide 23: Topics, Activities: 4
The next major topic is grain boundaries, whose crystallography can be easily characterized by electron microscopy
  We will discuss the physical characteristics of grain boundaries, e.g. energy, mobility, together with the additional complications for symmetry and descriptions (Rodrigues vectors, quaternions)
  The objective is for students to become familiar with both the properties of grain boundaries and the methods for quantitative characterization

## Slide 24: Topics, Activities: 5
The next major topic is microstructure-property relationships using texture information
  Students will explore percolation analysis using electrical conductivity in superconductors as an example of a case where the crystal properties are (strongly) anisotropic and the grain boundaries are also anisotropic.
  This exercise will teach students how to develop a computer model on a discrete grid. Programming will be required, although any of the following languages may be used: C, C++, Fortran, VisualBasic.

## Slide 25: Topics, Activities: 6
The next major topic is microstructural measurement and stereology. Stereology is the science of obtaining 3D information about microstructure from 2D sections.
  Even something as seemingly straightforward as grain size is interesting because we lack quantitative models for the size distribution. GSDs are approximately log-normal, but not exactly.
  Stereology is necessary because characterization is most readily available on plane cross sections. Therefore for most microstructures, we need tools to infer the true 3D image from the 2D slices through the material
  The objective is to equip students to understand and use stereological tools, e.g. reconstruction of particle size distributions from cross sections, or, use of Microstructure Builder

## Slide 26: Topics, Activities: 7
The next major topic is elastic and plastic anisotropy
  Plastic deformation in metals (and ceramics at high temperatures, and some polymers) is governed by the motion of line defects - dislocations. The crystallographically restricted slip directions (Burgers vector) and slip planes mean that any degree of texture results in an anisotropic response, e.g. a multi-axial strain from an imposed unixial stress
  The objective is to equip students to understand and use polycrystal analysis + modeling, e.g. LApp

## Slide 27: Lecture List (abbreviated)
1. Introduction
2. Texture components, Euler angles
3. X-ray diffraction
4. Calculation of ODs from pole figure data, popLA
5. Orientation distributions
6. Microscopy, SEM, electron diffraction
7. Texture in bulk materials
8. EBSD/OIM
9. Misorientation at boundaries
10. Continuous functions for ODs
11. Stereology
12. Graphical representation of ODs
13. Symmetry (crystal, sample)
14. Euler angles, variants
15. Volume fractions, Fiber textures
16. Grain boundaries
17. Rodrigues vectors, quaternions
18. CSL boundaries
19. GB properties
20. 5-parameter descriptions of GBs
21. Herring’s relations
22. Elastic, plastic anisotropy
23. Taylor/Bishop-Hill model
24. Yield Surfaces

## Slide 28: Learning Approach
Overall Concept
Phenomenology
Cause-and-Effect
Required Math+Physics+Chemistry
Measurement Technique, data
Analysis
Interpretation

## Slide 29: Anisotropy-Texture
Overall Concept: materials behave anisotropically and, regarding texture as part of microstructure, this is another microstructure-property relationship
Phenomenology: anisotropy is correlated with non-random grain alignment.
Cause-and-Effect: the cause of anisotropic behavior is the crystallographic preferred orientation (texture) of the grains in a polycrystal.
4. Required Math: Crystal orientation is described by a (3D) rotation; therefore texture requires distributions of rotations to be described.
Measurement Technique, data: see next page
6. Analysis: 3D distributions have to be reconstructed from 2D projections
7. Interpretation: Although pole figures often provide easily recognized patterns, orientation distributions provide quantitative information.

## Slide 30
<100>
{001}
<100>
{011}
Crystal Axes
Sample Axes
RD
TD
ND
Rotation 1 (φ1): rotate sample axes about ND
Rotation 2 (Φ): rotate sample axes about rotated RD
Rotation 3 (φ2): rotate sample axes about rotated ND
a
Euler Angles to represent a crystal orientation with respect to samples axes
C. N. Tomé and R. A. Lebensohn, Crystal Plasticity, presentation at Pohang University of Science and Technology, Korea, 2009
Component | RD | ND
Cube | <100> | {001}
Goss | <100> | {011}
Brass | <112> | {110}
Copper | <111> | {112}
100
010
001
Crystal Orientations – Euler angles

## Slide 31
<100>
{001}
<100>
{011}
Rotation 1 (φ1): rotate sample axes about ND
Rotation 2 (Φ): rotate sample axes about rotated RD
Rotation 3 (φ2): rotate sample axes about rotated ND
a
[1] C. N. Tome and R. A. Lebensohn, crystal plasticity, presentation at Pohang University of Science and Technology, Korea, 2009
Component | Euler Angles (°)
Cube | (0, 0, 0)
Goss | (0, 45, 0)
Brass | (35, 45, 0)
Copper | (90, 45, 45)
010
001
Crystal Orientations – Orientation Space
Φ
φ1
φ2
Cube {100}<001> (0, 0, 0)
Goss
{110}<001>
(0, 45, 0)
Brass
{110}<-112>
(35, 45, 0)
Orientation Space

## Slide 32
Φ
φ1
φ2
Cube {100}<001> (0, 0, 0)
Goss
{110}<001>
(0, 45, 0)
Brass
{110}<-112>
(35, 45, 0)
ODF gives the density of grains having a particular orientation.
Crystal Orientations – ODF
ODF
Orientation Distribution Function f (g)
g = {φ1, Φ, φ2}

## Slide 33: {111} Pole Figure for Rolled Cu
A {111} pole figure of rolled copper, showing the typical distribution of intensity for moderate to large strains. The rolling plane normal (ND) is perpendicular to the plane of the figure and the rolling (RD) and transverse (TD) directions are vertical and horizontal, respectively, in the plane of the figure. The contours indicate the diffracted intensity in units of Multiples of a Random Density (MRD). High frequencies of <111> directions are found close to the RD, for example, and also inclined 20° away from the ND towards the RD [Hirsch, J. and K. Lücke. Mechanism of Deformation and Development of Rolling Textures in Polycrystalline FCC Metals 1. Description of Rolling Texture Development in Homogeneous CuZn Alloys. Acta Metallurgica, 36 (11): 2863-2882, 1988].

## Slide 34: Effect of Alloying: Cu-Zn (brass); the texture transition
Zn content: (a) 0%, (b) 2.5%, (c) 5%, (d) 10%, (e) 20% and (f) 30% [Stephens 1968]
Copper
Brass
Check contour levels: 1, 2, 3 …?

## Slide 35: Texture: Quantitative Description
Three (3) parameters needed to describe the orientation [of a crystal relative to the embedding body or its environment] because it is a 3D rotation.
Most common description: 3 [rotation] Euler angles
Other descriptions include: (orthogonal) rotation matrix (or axis transformation matrix), Rodrigues-Frank vector, unit quaternion.
A common misunderstanding: although 2 parameters are sufficient to describe the position of a vector, a 3D object such as a crystal requires 3 parameters to describe its (angular) position
Most experimental methods [X-ray pole figures included] do not measure all 3 angles, so orientation distribution must be calculated. An orientation distribution is just a probability distribution: it tells you how likely you are to find a crystal that has the orientation specified by the coordinates (Euler angles) of the point

## Slide 36: Euler Angles, Animated
[010]
[100]
[001]
Crystal
e1=Xsample=RD
e2=Ysample=TD
e3=Zsample=ND
Sample Axes
RD
TD
e”2
e”3
=e”1
2nd position
ycrystal=e2’’’
f2
xcrystal=e1’’’
zcrystal=e3’’’ =
3rd position (final)
e’1
e’2
f1
e’3=
1st position
F

## Slide 37: Sections through an OD
f2 = 0°
f2 = 5°
f2 = 15°
f2 = 10°
f1
F
f2
This example of the texture of rolled copper, taken from Bunge’s book, uses the Bunge definition of the Euler angles so that each possible orientation is defined by (f1, , f2)

## Slide 38: Transformations of Axes
A 3D object such as a crystal requires 3 parameters to describe its (angular) position.
The 3 parameters can be one of a great variety of types, including Euler angles (best known in Materials Science), unit quaternions (popular in robotics), Rodrigues vectors (useful for grain boundaries), or rotation matrices.
Most often in materials science, we prefer to describe properties and field quantities (stress, strain, current, heat flux …) in terms of a convenient local frame.
Since some quantities are most easily described in, say, a frame associated with a specimen (e.g. rolling-transverse-normal) and others (such as single crystal properties) are associated with the local crystal frame, we need a method to transform quantities from one frame to another.
There is a standard procedure known as “transformation of axes” that we will use. Later on we will see that it is implicit in the Tensor Transformation Rule. Mathematicians know this as a “passive rotation”. It is complementary to the “active rotation” commonly used in solid mechanics.
Vector and Tensor Analysis, Borisenko & Tarapov, translated by R. Silverman,Dover 1979.

## Slide 39: Scalars, Vectors, Tensors: Notation
General case: three dimensions
Vector: needs 3 numbers or coefficients to quantify its x, y and z components.
Two notations for vectors: “vector-tensor notation” where bold-face implies higher-than-scalar nature; “component notation” where a suffix(-es) show how many coefficients are needed.
Vector: either b or bi,i{1,2,3}, or, i{x,y,z}.
2nd rank tensor: either T or Tij, i,j{1,2,3}
Advantage of vector-tensor notation is that the equations work (or, are valid) in any reference frame. By contrast, when component notation is used, the actual values of the coefficients depend on which reference frame is used.
If you see subscripts attached to a quantity, it is (almost always) a tensor and the Einstein summation convention is assumed. The Einstein summation convention says that a repeated index (on the RHS) implies summation over that index (typically 1,2, and 3 in 3D). If the same, non-repeated index is found on both sides of an equation, then no summation is performed.

## Slide 40: Changing the Coordinate System
Many different choices are possible for the orthonormal base vectors and origin of the Cartesian coordinate system. A vector is an example of an entity which is independent of the choice of coordinate system. Its direction and magnitude must not change (and are, in fact, invariants), although its components will change with this choice.
Why would we want to do something like this? For example, although the properties are conveniently expressed in a crystal reference frame, experiments often place the crystals in a non-symmetric position with respect to an experimental frame. Therefore we need some way of converting the coefficients of the property into the experimental frame.
Changing the coordinate system is also known as axis transformation.

## Slide 41: Motivation for Axis Transformation
One motivation for axis transformations is the need to solve problems where the specimen shape (and the stimulus direction) does not align with the crystal axes. Consider what happens when you apply a force parallel to the sides of this specimen …
[100]
[110]
The direction parallel to the long edge does not line up with any simple, low index crystal direction. Therefore we have to find a way to transform the properties that we know for the material into the frame of the problem (or vice versa).
Image of Pt surface from www.cup.uni-muenchen.de/pc/wintterlin/IMGs/pt10p3.jpg
Applied stress

## Slide 42
Consider a new orthonormal system consisting of right-handed base vectors: These all have the same origin, o, associated with the original axes:
The vector v is clearly expressed equally well in either coordinate system: Note - same physical vector but different values of the components.
We need to find a relationship between the two sets of components for the vector.
New Axes

## Slide 43: Direction cosines
q1
q2
q3
a1 = u = cosq1
a2 = v = cosq2
a3 = w = cosq3
a2
Each direction cosine is the length of the unit vector, a, projected onto each axis in turn. The second direction cosine, a2 is shown.

## Slide 44: Rotation of axes in the x-y plane
x
y
q
x’
y’
v
x, y = old axes; x’,y’ = new axes
Passive Rotation/ Transformation of Axes
General rule for determining the coefficients of a transformation matrix, using dot-products:

## Slide 45: Example: rotation angle = 30°
q
x’
y’
v
x, y = old axes; x’,y’ = new axes
Passive Rotation/ Transformation of Axes

## Slide 46: Tensor: definition, contd.
In order for a quantity to “qualify” as a tensor it has to obey the axis transformation rule, as discussed in the previous slides.
The transformation rule defines relationships between transformed and untransformed tensors of various ranks. Vector: V’i = aijVj 2nd rank T’ij = aikajlTkl 3rd rank T’ijk = ailajmaknTlmn 4th rank T’ijkl = aimajnakoalpTmnop
This rule is a critical piece of information, which you must know how to use.

## Slide 47: 3D Axis Transformation
e1
^
e’1
^
e2
^
e’2
^
e3
^
e’3
^
Sample to Crystal (primed)
Obj/notation AxisTransformation Matrix EulerAngles Components
e = old (sample) axes; e’ = new (crystal) axes

## Slide 48: Rodrigues-Frank vector definition
We write the axis-angle representation as: where the rotation axis = OQ/|OQ|
The Rodrigues vector is defined as:
The vector is parallel to the rotation axis, and the rotation angle is , and the magnitude of the vector is scaled by the tangent of the semi-angle.

## Slide 49: Quaternion: definition
q = q(q1,q2,q3,q4)
For a unit quaternion, representing a rotation, we have: q(r sinq/2, cosq/2) q(u sinq/2, v sinq/2, w sinq/2, cosq/2)
Here, the rotation axis is r=[u,v,w], as a unit vector, and the rotation angle is .
Alternative notation puts cosine term in 1st position, q(q0,q1,q2,q3) : q = (cosq/2, u sinq/2, v sinq/2, w sinq/2).

## Slide 50: Summary
Microstructure contains far more than qualitative descriptions (images) of cross-sections of materials.
Most properties are anisotropic which means that it is critically important for quantitative characterization to include orientation information (texture).
Many properties can be modeled with simple relationships, although numerical implementations are (almost) always necessary.

## Slide 51: Supplemental Slides

## Slide 52: Websters’ Dictionary, texture
    Pronunciation: 'teks-ch&r
    Function: noun
    Etymology: Latin textura, from textus, past participle of texere to weave -- more at TECHNICAL
    Date: 1578
    1 a : something composed of closely interwoven elements; specifically : a woven cloth b : the structure formed by the threads of a fabric
    2 a : essential part : SUBSTANCE b : identifying quality : CHARACTER
    3 a : the disposition or manner of union of the particles of a body or substance b : the visual or tactile surface characteristics and appearance of something <the texture of
    an oil painting>
    4 a : a composite of the elements of prose or poetry <all these words... meet violently to form a texture impressive and exciting -- John Berryman> b : a pattern of
    musical sound created by tones or lines played or sung together
    5 a : basic scheme or structure b : overall structure

## Slide 53: What do we need to learn?
1. How to measure texture:
  Method 1: x-ray pole figures
  Method 2: electron back scatter diffraction (EBSD)
  Method 3: transmission electron microscopy (TEM)
  Stereology: sections through 3D materials
2. What causes texture to develop in materials, and how does it depend on material type and the processing history?
  Deformation of bulk metals: rolling vs. torsion etc.
  Annealing: grain growth, recrystallization
  Thin films

## Slide 54: What do we need to learn? (contd.)
3. How to describe texture quantitatively, how to plot textures, and how to understand texture:
  Method 1: pole figures
  Method 2: orientation distributions (OD)
  Symmetry: crystal symmetry, sample symmetry
  Components
  Fibers
  How to obtain ODs from pole figures
4. How does anisotropy depend on texture?
  Elastic anisotropy
  Plastic anisotropy; yield surfaces
  Corrosion (grain boundaries)

## Slide 55: What do we need to learn? (contd.)
5. Grain Boundaries
  Grain boundary atomic structure: low angle vs. high angle boundaries
  Special grain boundaries: Coincident Site Lattice boundaries (CSL)
  How to describe grain boundary crystallography: axis-angle, Rodrigues vectors
  How to measure grain boundaries
6. Underlying Concepts
  Different descriptions of rotations: Miller indices, Euler angles, matrices, axis-angle pairs, Rodrigues vectors, quaternions
  How to work with distributions
  Spherical harmonics (series expansions)
  Discretization of distributions
  Volume fractions

## Slide 56: Learning Approach: 1
What is the result that we want? For a solved problem, we quote the equation or concept.
How do we set up the differential equations?
How do we find solutions for the differential equations, and what are they?
How do we determine the boundary conditions?
How do we visualize the solution - what graphs are appropriate?
What do worked solutions corresponding to physical situations look like?
What are the variables?

## Slide 57: How to Measure Texture
X-ray diffraction; pole figures; measures average texture at a surface (µms penetration); projection (2 angles).
Neutron diffraction; type of data depends on neutron source; measures average texture in bulk (cms penetration in most materials) ; projection (2 angles).
Electron [back scatter] diffraction; easiest [to automate] in scanning electron microscopy (SEM); local texture; complete orientation (3 angles).
Optical microscopy: optical activity (plane of polarization); limited information (one angle)

## Slide 58: X-ray Pole Figures
X-ray pole figures are the most common source of texture information; cheapest, easiest to perform.
Pole figure:= variation in diffracted intensity with respect to direction in the specimen.
Representation:= map in projection of diffracted intensity.
Each PF is equivalent to a geographic map of a hemisphere (North pole in the center).
Map of crystal directions w.r.t. sample reference frame.

## Slide 59: Anisotropy Example 2: Drawn Aluminum Cup with Ears
Randle, Engler, p.340
Figure shows example of a cup that has been deep drawn. The plastic anisotropy of the aluminum sheet resulted in non-uniform deformation and “ears.”

## Slide 60: Challenges in Microstructure
Annealing textures: where does the cube texture come from in annealed fcc metals? Goss texture in bcc metals?
Processing: how can we produce large crystals of ceramics by abnormal grain growth?
Plastic deformation: how can we explain the “break-up” of grains during deformation?
Simulation, numerical representation: how can we generate faithful 3D representations of microstructure?
Constitutive relations: what are the properties of defects such as grain boundaries?

## Slide 61: Notation: vectors, matrices
Vector-Matrix: v is a vector, A is a matrix (always a square matrix in this course).
Index notation: explicit indexes (Einstein convention): vi is a vector, Ajk is a matrix (maybe tensor, though not necessarily).
Scalar (dot) product: c = a•b = aibi; zero dot product means vectors are perpendicular. For two unit vectors, the dot product is equal to the cosine of the angle between them.
Vector (cross) product: c = ci = a x b = a  b = eijk ajbk; generates a vector that is perpendicular to the first two. Two vectors that are perpendicular have a zero length cross product. The cross product defines a rotation axis that carries one vector into another. The magnitude of the cross product is the product of the magnitudes (lengths) of the vectors multiplied by the sine of the angle between them.
Permutation or alternating tensor, ijk, is +1 for ijk=123, 231, 312, and -1 for ijk= 132, 213 and 321.
Obj/notation AxisTransformation Matrix EulerAngles Components

## Slide 62: An axis system
Consider a right-handed set of axes defined by a set of three unit basis vectors, e.
Right-handed means that the scalar triple product, e1xe2•e3 = +1
o

## Slide 63: Direction cosines
x1
x2
x3
q1
q2
q3
a1 = u = cosq1
a2 = v = cosq2
a3 = w = cosq3
a

## Slide 64
Consider a new orthonormal system consisting of right-handed base vectors with the same origin, o, associated with the basis vectors. The vector is clearly expressed equally well in either coordinate system: Note - same vector, different values of the components. We need to find a relationship between the two sets of components for the vector.
New Axes

## Slide 65
The two systems are related by the nine direction cosines, aij, which fix the cosine of the angle between the ith primed and the jth unprimed base vectors: Equivalently, aij represent the components of in according to the expression
Direction Cosines: definition

## Slide 66: Rotation of axes in the x-y plane
x
y
q
x’
y’
v
x, y = old axes; x’,y’ = new axes
Passive Rotation/ Transformation of Axes

## Slide 67: Example: rotation angle = 30°
x
y
q
x’
y’
v
x, y = old axes; x’,y’ = new axes
Passive Rotation/ Transformation of Axes

## Slide 68: Rotation Matrices
Since an orthogonal matrix merely rotates a vector but does not change its length, the determinant is one, det(a)=1.
Moreover, each row and each column is a unit vector, so these six relations apply, resulting in only 3 independent parameters:

## Slide 69: Scalars, Vectors, Tensors
Scalar:= quantity that requires only one number, e.g. density, mass, specific heat.
Vector:= quantity that has direction as well as magnitude, e.g. velocity, current, magnetization; requires 3 numbers or coefficients (in 3D).
Tensor:= quantity that requires higher order descriptions but is the same, no matter what coordinate system is used to describe it, e.g. stress, strain, elastic modulus; requires 9 (or more, depending on rank) numbers or coefficients.

## Slide 70: Scalars, Vectors, Tensors: NOTATION
General case: three dimensions
Vector: needs 3 numbers or coefficients to quantify its x, y and z components.
Two notations for vectors: “vector-tensor notation” where bold-face implies higher-than-scalar nature; “component notation” where a suffix(-es) show how many coefficients are needed.
Vector: either b or bi,i  {1,2,3}, or, i  {x,y,z}.
2nd rank tensor: either T or Tij, i,j  {1,2,3}
Advantage of vector-tensor notation is that the equations work in any reference frame. By contrast, when component notation is used, the actual values of the coefficients depend on which reference frame is used.
If you see subscripts attached to a quantity, it is (almost always) a tensor and the Einstein summation convention is assumed. The Einstein summation convention says that a repeated index (on the RHS) implies summation over that index (typically 1,2, and 3 in 3D).