## Slide 1: Plastic Deformation of Single Crystals
27-750
Texture, Microstructure & Anisotropy
A.D. Rollett
With thanks to Prof. H. Garmestani (GeorgiaTech), G. Branco (FAMU/FSU)
Last revised: 11th Feb. ‘14
Notes: Be sure to also read the section in the popLA manual (popLA.manual.pdf] that discusses the use of Lapp, p47 et seq. This description is admittedly brief and does not discuss the sensitivity of the results to the choices made.

## Slide 2: Objective
The objective of this lecture is to explain how single crystals deform plastically.
Subsidiary objectives include:
  Schmid Law
  Critical Resolved Shear Stress
  Lattice reorientation during plastic deformation
Note that this development assumes that we load each crystal under stress boundary conditions. That is, we impose a stress and look for a resulting strain (rate).

## Slide 3: Why is the Schmid factor useful?
The Schmid factor is a good predictor of which slip or twinning system will be active, especially for small plastic strains (< 5 %).
It has been used to analyze the plasticity of ordered intermetallics, especially Ni3Al and NiAl.
It has been used to analyze twinning in hexagonal metals, which is an essential deformation mechanism.
Some EBSD software packages will let you produce maps of Schmid factor.
Schmid factor has proven useful to visualize localization of plastic flow as a precursor to fatigue crack formation.
Try searching with “Schmid factor” (include the quotation marks).

## Slide 4: Bibliography
U.F. Kocks, C. Tomé, H.-R. Wenk, Eds. (1998). Texture and Anisotropy, Cambridge University Press, Cambridge, UK: Chapter 8, Kinematics and Kinetics of Plasticity.
C.N. Reid (1973). Deformation Geometry for Materials Scientists. Oxford, UK, ISBN: 1483127249, Pergamon.
Khan and Huang (1999), Continuum Theory of Plasticity, ISBN: 0-471-31043-3, Wiley.
W. Hosford, (1993), The Mechanics of Crystals and Textured Polycrystals, Oxford Univ. Press.
G.E. Dieter (1986), Mechanical Metallurgy, ISBN: 0071004068, McGraw-Hill.
J.F. Nye (1957). Physical Properties of Crystals. Oxford, Clarendon Press.
T. Courtney, Mechanical Behavior of Materials, McGraw-Hill, 0-07-013265-8, 620.11292 C86M.

## Slide 5: Notation
Strain (tensor), local: Elocal; global: Eglobal
Slip direction (unit vector): b (or m)
Slip plane (unit vector) normal: n (or s)
Stress (tensor): s
Shear stress (scalar, usually on a slip system): t
Angle between tensile axis and slip direction: 
Angle between tensile axis and slip plane normal: 
Schmid factor (scalar): m
Slip system geometry matrix (3x3): m
Taylor factor (scalar): M
Shear strain (scalar, usually on a slip system): g
Stress deviator (tensor): S
Rate sensitivity exponent: n
Slip system index: s (or )
Set of Reference Axes: Oxi

## Slide 6: Historical Development
Physics of single-crystal plasticity
Established by Ewing and Rosenhaim(1900), Polanyi(1922), Taylor and others(1923/25/34/38), Schimd(1924), Bragg(1933)
Mathematical representation
Initially proposed by Taylor in 1938, followed by Bishop & Hill (1951)
Further developments by Hill(1966), Kocks (1970), Hill and Rice(1972) , Asaro and Rice(1977), Hill and Havner(1983)

## Slide 7
Experimental measurements showed that:
At room temperature the major source for plastic deformation is the dislocation motion through the crystal lattice
Dislocation motion occurs on fixed crystal planes (“slip planes”) in fixed crystallographic directions (corresponding to the Burgers vector of the dislocation that carries the slip)
The crystal structure of metals is not altered by the plastic flow
Volume changes during plastic flow are negligible, which means that the pressure (or, mean stress) does not contribute to plasticity
Physics of Slip
Experimental technique
Uniaxial Tension or Compression

## Slide 8
Shear Stress – Shear Strain Curves
A typical flow curve (stress-strain) for a single crystal shows three stages of work hardening:
Stage I = “easy glide” with low hardening rates ~µ/10000; - Stage II with high, constant (linear) hardening rate ~µ/200, nearly independent of temperature or strain rate; - Stage III with decreasing hardening rate and very sensitive to temperature and strain rate. Dynamic recovery operates;
Stage IV (not shown) with low hardening rates ~µ/10000.
Hardening behavior will be discussed in another lecture.

## Slide 9: Burgers vector: b
Screw position: line direction//b
Edge position: line directionb
A dislocation is a line defect in the crystal lattice. The defect has a definite magnitude and direction determined by the closure failure in the lattice found by performing a circuit around the dislocation line; this vector is known as the Burgers vector of the dislocation. It is everywhere the same regardless of the line direction of the dislocation. Dislocations act as carriers of strain in a crystal because they are able to change position by purely local exchange in atom positions (conservative motion) without any long range atom motion (i.e. no mass transport required).
[Reid]

## Slide 10: Slip steps
Slip steps (where dislocations exit from the crystal) on the surface of compressed single crystal of Nb.
[Reid]

## Slide 11: Dislocation glide
The effect of dislocation motion in a crystal: passage causes one half of the crystal to be displaced relative to the other. This is a shear displacement, giving rise to a shear strain.
[Dieter]

## Slide 12: Single Crystal Deformation
To make the connection between dislocation behavior and yield strength as measured in tension, consider the deformation of a single crystal.
Given an orientation for single slip, i.e. the resolved shear stress reaches the critical value on one system ahead of all others, then one obtains a “pack-of-cards” straining.
[Dieter]

## Slide 13: Resolved Shear Stress
Geometry of slip: how big an applied stress is required for slip?
To obtain the resolved shear stress based on an applied tensile stress, P, take the component of the stress along the slip direction which is given by Fcosl, and divide by the area over which the (shear) force is applied, A/cosf. Note that the two angles are not complementary unless the slip direction, slip plane normal and tensile direction happen to be co-planar. t = (F/A) coslcosf = s coslcosf = s * m
Schmid factor := m
In tensor (index) form:
 = bi ij nj
= b
= n

## Slide 14: Schmid’s Law
Initial yield stress varies from sample to sample depending on, among several factors, the position of the crystal lattice relative to the loading axis.
It is the shear stress resolved along the slip direction on the slip plane that initiates plastic deformation.
Yield will begin on a slip system when the shear stress on this system first reaches a critical value (critical resolved shear stress, crss), independent of the tensile stress or any other normal stress on the lattice plane.
Schmid postulated that:
E. Schmid & W. Boas (1950), Plasticity of Crystals, Hughes & Co., London.

## Slide 15: Schmid’s Law
Resolved Shear Stress

## Slide 16: Critical Resolved Shear Stress
The experimental evidence of Schmid’s Law is that there is a critical resolved shear stress. This is verified by measuring the yield stress of single crystals as a function of orientation. The example below is for Mg which is hexagonal and slips most readily on the basal plane (all other tcrss are much larger).
“Soft orientation”, with slip plane at 45°to tensile axis
“Hard orientation”, with slip plane at ~90°to tensile axis
s = t/coslcosf
Exercise: draw a series of diagrams that illustrate where the tensile axis points in relation to the basal plane normal for different points along this curve

## Slide 17: Calculation of Resolved Shear Stress
Using Schmid’s law

## Slide 18
Rotation of the Crystal Lattice
The slip direction rotates towards the tensile axis
[Khan]

## Slide 19: FCC Geometry of Slip Systems
[Reid]
In fcc crystals, the slip systems are combinations of <110> slip directions (the Burgers vectors) and {111} slip planes.

## Slide 20
Slip Systems in fcc materials
For FCC materials there are 12 slip systems (with + and - shear directions:
Four {111} planes, each with
three <011> directions: the letter denotes the plane, and the subscript number denotes the direction (in that plane).
[Khan]
The combination of slip plane {a,b,c,d} and slip direction {1,2,3} that operates within each unit triangle is shown in the figure
Note correction to system b2

## Slide 21: Geometry of Single Slip
For tensile stress applied in the [100]-[110]-[111] unit triangle, the most highly stressed slip system (highest Schmid factor) has a (11-1) slip plane and a [101] slip direction (the indices of both plane and direction are the negative of those shown on the previous page).
Caution: this diagram places [100] in the center, not [001].
[Hosford]

## Slide 22: Schmid factors
The Schmid factors, m, vary markedly within the unit triangle (a). One can also (b) locate the position of the maximum (=0.5) as being equidistant between the slip plane and slip direction.
(a)
(b)
[Hosford]

## Slide 23: Names of Slip Systems
In addition to the primary slip system in a given triangle, there are systems with smaller resolved shear stresses. Particular names are given to some of these. For example the system that shares the same Burgers vector allows for cross-slip of screws and so is known as the cross slip system. The system in the triangle across the [100]-[111] boundary is the conjugate slip system.
[Hosford]

## Slide 24
Rotation of the Crystal Lattice in Tensile Test of an fcc Single Crystal
The tensile axis rotates in tension towards the [100]-[111] line. If the tensile axis is in the conjugate triangle, then it rotates to the same line so there is convergence on this symmetry line. Once on the line, the tensile axis will rotate towards [211] which is a stable orientation. Note: the behavior in multiple slip is similar but there are significant differences in terms of the way in which the lattice re-orients relative to the tensile axis.
[Hosford]

## Slide 25
Rotation of the Crystal Lattice in Compression Test of an fcc Single Crystal
The slip plane normal rotates towards the compression axis
[Khan]

## Slide 26: Useful Equations
To find a new plane normal, P, based on an initial plane normal, p, after slip, use the following:
[Reid]
Following the notation in Reid: n:= slip plane normal (unit vector); b:= slip direction (unit vector).
To find a new direction, D, based on an initial direction, d, after slip, use (and remember that crystal directions do not change):

## Slide 27: Taylor rate-sensitive model
We will find out later that the classical Schmid Law picture of elastic-perfectly plastic behavior is not sufficient.
In fact, there is a smooth transition from elastic to plastic behavior that can be described by a power-law behavior.
The shear strain rate on each slip system is given by the following (for a specified stress state), where* mij = binj, or m=b⊗n:
* “m” is a slip tensor, formed as the outer product of the slip direction and slip plane normal

## Slide 28: Schmid Law Calculations
To solve problems using the Schmid Law, use this pseudo-code:
  Check that single slip is the appropriate model to use (as opposed to, say, multiple slip and the Taylor model);
  Make a list of all 12 slip systems with slip plane normals (as unit vectors) and slip directions (as unit vectors that are perpendicular to their associated slip planes; check orthogonality by computing dot products);
  Convert whatever information you have on the orientation of the single crystal into an orientation matrix, g;
  Apply the inverse of the orientation to all planes and directions so that they are in specimen coordinates;
  If the tensile stress is applied along the z-axis, for example, compute the Schmid factor as the product of the third components of the transformed plane and direction;
  Inspect the list of absolute values of the Schmid factors: the slip system with the largest absolute value is the one that will begin to slip before the others;
  Alternatively (for a general multi-axial state of stress), compute the following quantity, which resolves/projects the stress, , onto the kth slip system:

## Slide 29: Hexagonal Metals
For typical hexagonal metals, the primary systems are: Basal slip {0001}<1-210> Prismatic slip {10-10}<1-210> Pyramidal twins {10-11}<1-210>
At room temperature and below for Zr, the systems are: Prismatic slip {10-10}<1-210> Tension twins {10-12}<10-11>, and {11-21}<-1-126> Compression twin {11-22}<-1-123> Also secondary pyramidal slip may play a limited role at RT: {10-11}<-2113>, or {11-21}<-2113>

## Slide 30: Summary
The Schmid Law is well established for the dependence of onset of plastic slip as well as the geometry of slip.
Cubic metals have a limited set of slip systems: {111}<110> for fcc, and {110}<111> for bcc (neglecting pencil glide for now).
Hexagonal metals have a larger range of slip systems (see previous slide).

## Slide 31: Supplemental Slides

## Slide 32: Crystal Planes in HCP
Basal
(0002)
Pyramidal
(1 0 -1 1)
Prism
(0 -1 1 0)
(2 -1 -1 0)
Pyramidal
(1 0 -1 2)
Berquist & Burke: Zr alloys
Also: Was: fig. 14.19

## Slide 33: Crystal Directions in HCP
[0002]
Unique direction in HCP material is [0002].
This direction is perpendicular to the basal plane (0002).
Useful for basic texture quantification.
Berquist & Burke: Zr alloys

## Slide 34: Dislocation Motion
Dislocations control most aspects of strength and ductility in structural (crystalline) materials.
The strength of a material is controlled by the density of defects (dislocations, second phase particles, boundaries).
For a polycrystal: syield = <M> tcrss = <M> a G b √r

## Slide 35: Dislocations & Yield
Straight lines are not a good approximation for the shape of dislocations, however: dislocations really move as expanding loops.
The essential feature of yield strength is the density of obstacles that dislocations encounter as they move across the slip plane. Higher obstacle density  higher strength.
[Dieter]

## Slide 36: Why is there a yield stress?
One might think that dislocation flow is something like elasticity: larger stresses imply longer distances for dislocation motion. This is not the case: dislocations only move large distances once the stress rises above a threshold or critical value (hence the term critical resolved shear stress).
[Dieter]
Consider the expansion of a dislocation loop under a shear stress between two pinning points (Frank-Read source).

## Slide 37: Orowan bowing stress
If you consider the three consecutive positions of the dislocation loop, it is not hard to see that the shear stress required to support the line tension of the dislocation is roughly equal for positions 1 and 3, but higher for position 2. Moreover, the largest shear stress required is at position 2, because this has the smallest radius of curvature. A simple force balance (ignoring edge-screw differences) between the force on the dislocation versus the line tension force on each obstacle then gives tmaxbl = (µb2/2), where l is the separation between the obstacles (strictly speaking one subtracts their diameter), b is the Burgers vector and G is the shear modulus (Gb2/2 is the approximate dislocation line tension).

## Slide 38: Orowan Bowing Stress, contd.
To see how the force balance applies, consider the relationship between the shape of the dislocation loop and the force on the dislocation.
Line tension = Gb2/2 Force resolved in the vertical direction = 2cosf Gb2/2 Force exerted on the dislocation per unit length (Peach-Koehler Eq.) = tb Force on dislocation per obstacle (only the length perpendicular to the shear stress matters) = ltb
At each position of the dislocation, the forces balance, so t = cosf Gb2/lb
The maximum force occurs when the angle f = 0°, which is when the dislocation is bowed out into a complete semicircle between the obstacle pair.
t
l
Gb2/2
Gb2/2
f
t
l
Gb2/2
Gb2/2
f=0°
MOVIES: http://www.gpm2.inpg.fr/axes/plast/MicroPlast/ddd/

## Slide 39: Critical stress
It should now be apparent that dislocations will only move short distances if the stress on the crystal is less than the Orowan bowing stress. Once the stress rises above this value then any dislocation can move past all obstacles and will travel across the crystal or grain.
This analysis is correct for all types of obstacles from precipitates to dislocations (that intersect the slip plane). For weak obstacles, the shape of the critical configuration is not the semi-circle shown above (to be discussed later) - the dislocation does not bow out so far before it breaks through.

## Slide 40: Stereology: Nearest Neighbor Distance
The nearest neighbor distance (in a plane), ∆2, can be obtained from the point density in a plane, PA.
The probability density, P(r), is given by considering successive shells of radius, r: the density is the shell area, multiplied by the point density , PA, multiplied by the remaining fraction of the cumulative probability.
For strictly 1D objects such as dislocations, ∆2 may be used as the mean free distance between intersection points on a plane.
r
dr
Ref: Underwood, pp 84,85,185.

## Slide 41: Dislocations as obstacles
Dislocations can be considered either as a set of randomly oriented lines within a crystal, or as a set of parallel, straight lines. The latter is easier to work with whereas the former is more realistic.
Dislocation density, r, is defined as either line length per unit volume, LV. It can also be defined by the areal density of intersections of dislocations with a plane, PA.
Randomly oriented dislocations: use r = LV = 2PA; ∆2 = (2PA)-1/2; thus l = (2√{LV/2})-1  (2√{r/2})-1. l is the obstacle spacing in any plane.
Straight, parallel dislocations: use r = LV = PA where PA applies to the plane orthogonal to the dislocation lines only; ∆2=(PA)-1/2; thus l = 1/√LV  1/√r where l is the obstacle spacing in the plane orthogonal to the dislocation lines only.
Thus, we can write tcrss = aµb√r
q”