## Slide 1
Textures in Thermomechanical Processing (TMP) of Metals
Last revised: 26th Apr. 2016
A. D. Rollett
27-750 Texture, Microstructure & Anisotropy

## Slide 2: Objectives
Introduce you to experimentally observed textures in a wide range of materials.
Develop a taxonomy of textures based on deformation type.
Prepare you for relating observed textures to theoretical (numerical) models of texture development, especially the Taylor model.
See chapter 5 in Kocks, Tomé & Wenk.
Some slides courtesy of Prof. P. Kalu (FAMU) and Prof. D. Waryoba (Penn State Dubois)

## Slide 3: Taxonomy
Note that solidification often introduces texture where the microstructure is columnar because it is usually dendritic and the preferred growth direction is <100>. Equi-axed microstructures are nearly random.
Deformation history more significant than alloy.
Crystal structure determines texture through slip (and twinning) characteristics.
Alloy (and temperature) can affect textures through planarity of slip.
Annealing (recrystallization) sometimes produces a drastic change in texture, especially in pure fcc metals.

## Slide 4: Why does deformation result in texture development?
Qualitative discussion:
Deformation means that a body changes its shape, which is quantified by the plastic strain, ep.
Plastic strain is accommodated in crystalline materials by dislocation motion, or by re-alignment of long chain molecules in polymers.

## Slide 5: Dislocation glide ⇒ grain reorientation
Dislocation motion at low (homologous) temperatures occurs by glide of loops on crystallographic planes in crystallographic directions: restricted glide.
Restricted glide throughout the volume is equivalent to uniform shear.
In general, shear requires lattice rotation in order to maintain grain alignment: compatibility is required, which is the basis for the Taylor model.

## Slide 6: Re-orientation  Preferred orientation
Reorientations experienced by grains depend on the type of strain (compression versus rolling, e.g.) and the type of slip (e.g. {111}<110> in fcc).
In general, some orientations are unstable (f(g) decreases) and some are stable (f(g) increases) with respect to the deformation imposed, hence texture development.

## Slide 7: The Taylor model
The Taylor model has one basic assumption: the change in shape (micro-strain) of each grain is identical to the body’s change in shape (macro-strain).
Named for G.I. Taylor, English physicist, mid-20th century; first to provide a quantitative explanation of texture development.

## Slide 8: The Taylor model
The Taylor model has one basic assumption: the change in shape (micro-strain) of each grain is identical to the body’s change in shape (macro-strain).
Named for G.I. Taylor, English physicist, mid-20th century; first to provide a quantitative explanation of texture development.
This was discussed in the lecture on multiple slip (L11).
Taylor G (1938) "Plastic strain in metals", J. Inst. Metals (U.K.) 62 307

## Slide 9: Single slip models ineffective
Elementary approach to single crystal deformation emphasizes slip on a single deformation system.
Polycrystal texture development requires multiple slip systems (5 or more, as dictated by von Mises).
Cannot use simple rules, e.g., alignment of slip plane with compression plane!

## Slide 10: Deformation systems (typical)
Fcc metals (low temperature): {111}<110>
Bcc metals: {110}<111>, {112}<111>, {123}<111>, pencil glide
Hexagonal metals: {1010}<1210>; prismatic {0001}<1210>; basal {1012}<1011>twin; {1011}<1123>; pyramidal, or c+a {2112}<2113>twin.

## Slide 11: Deformation systems (typical)
In deformed materials, texture or preferred orientation exists due to the anisotropy of slip. While slip in bcc metals generally occurs in the <111> type direction, it may be restricted to {110} planes or it may involve other planes. In general, texture development in bcc metals appears to involve <111>{112} as well as <111>{110}, but this may reflect easy cross-slip between different {110} planes, not actual {112} slip planes. (T. H. Courtney, Mechanical Behavior of Materials, McGraw-Hill, New York, 1990.)

## Slide 12: Strain Measures
Strain commonly defined as a scalar measure of (plastic, irreversible) deformation: logarithmic strain:= e = ln {lnew/lold}
Rolling strain: typical: reduction in thickness:= r = 100% x hnew/hold better to use von Mises equivalent strain: evM = 2/√3 ln {lold/lnew}

## Slide 13: Deformation Modes: sample symmetry
Tension, Wire Drawing, Extrusion C
Compression, Upsetting C
Torsion, Shear 2
Plane Strain Compression, Rolling mmm
Deformation modes of uniaxial type generate fiber textures, i.e. a single common crystal axis parallel to the deformation axis
Shear gives monoclinic symmetry
Plane strain gives orthorhombic symmetry

## Slide 14: Axisymmetric deformation: Extrusion, Drawing
a is the "die angle"; smaller angles give more uniform deformation but higher friction forces

## Slide 15: Uniaxial Strain
tension
compression
C
Inverse Pole Figures (FCC)
See Ch. 5 in Kocks, Tomé & Wenk

## Slide 16: Uniaxial Modes - C
Deformation mode/ fcc/ bcc/ hcp (Ti)
Wire drawing, <111> <110> <10-10>
Round extrusion. & <100>
Upsetting, <110> <111> <0001>
Uniaxial compression. &<100>
Note exchange of types between fcc & bcc

## Slide 17
In fcc metals, axisymmetric deformation (e.g. wire drawing) produces fiber texture: <111> + <100> duplex, parallel to the wire.
Schmid and Wassermann (1963): 60% <111> + 40% <100>
Ahlborn and Wassermann (1963): 66% <111> + 34% <100>
Electrolytic Copper
}
McHargue et al., 1959
Axisymmetric deformation

## Slide 18
Axisymmetric deformation
Axisymmetric deformation ~ higher order symmetry, C
Texture can be represented by an inverse pole figure (IPF).
In IPF, contour lines show the frequency with which the various directions, <uvw>, in the crystal coincide with the specimen axis under consideration
DD
TD
ND
DD – Drawing direction corresponds to RD in rolling

## Slide 19
The relative proportions of the two components are determined by the stacking fault energy and vary in a complex manner.
Axisymmetric deformation
English & Chin (1965) Acta metall.

## Slide 20
Effect of deformation strain
001
101
111
001
101
111
001
101
111
Max = 6.9
Max = 7.7
Max = 5.3
 = 2.80
 = 3.10
 = 3.56
001
101
111
001
101
111
001
101
111
111
001
101
Max = 4.1
Max = 4.5
Max = 5.0
Max = 5.4
 = 0.0
 = 0.45
 = 1.29
 = 2.31
D. R. Waryoba, Ph. D. Dissertation, FSU, 2003
X-ray IPFs showing the effect of strain on the texture of OFHC copper wire

## Slide 21
Max. = 5.29
Max. = 6.85
Max. = 2.06
Max. = 2.10
Max. = 2.48
Max. = 2.44
Max. = 4.65
Max. = 5.97
RT
180°C
250°C
300°C
450°C
500°C
600°C
750°C
X-ray IPFs showing the effect of annealing temperature on the texture of OFHC copper wire, initially drawn to true strain of 2.31. The strong <111> fiber first decreases with annealing temperature but then increases again.
D. R. Waryoba and P. N. Kalu, TMS 2003,San Diego, CA
Effect of Temperature

## Slide 22: Uniaxial Compression: various fcc metals
Initial texture theoretical texture exptl. texture
[Kocks Ch. 5: Inverse Pole Figures]

## Slide 23: BCC uniaxial textures
92% rolled Ta Tensile test in original RD to strain of 0.6: <110> fiber
(a) Normal and rolling direction inverse pole figures (equal area projection) of 92% rolled Ta and (b) Prior normal and rolling direction inverse pole figures for (a) tested in tension to a strain of 0.6 (tensile direction coincident to prior rolling direction).
Kocks, Ch. 5

## Slide 24
Texture inhomogeneity in Drawn Wires
III
II
I
Max = 4.2
Max = 3.5
Max = 15.7
OIM IPFs representing outer region, mid region, and inner core of the OFHC Cu wire drawn to true strain of 2.31 (contours are at 1, 2, 3 … times random)
D. R. Waryoba and P. N. Kalu, TMS 2005, San Francisco, CA

## Slide 25
Max = 9.2
Max = 5.3
Max = 5.1
10 min
OIM IPFs representing outer region, mid region, and inner core of the OFHC Cu wire drawn to true strain of 2.31 and annealed at 250°C for 10 min (contours are at 1, 2, 3 … times random)
Texture inhomogeneity in Drawn Wires
D. R. Waryoba and P. N. Kalu, TMS 2005, San Francisco, CA

## Slide 26: Rolling = Plane Strain
RD
ND
Rolling ~ plane strain deformation means extension or compression in a pair of directions with zero strain in the third direction: a multiaxial strain.

## Slide 27: Plane strain (rolling)
Plane strain means extension/compression in a pair of directions with zero strain in the third direction: a multiaxial strain.
tension
compression
3
1

## Slide 28: Typical rolling texture in FCC Materials
Type | Component | {hkl}<uvw> | Euler Angles (Bunge) |  | 
 |  |  | 1 |  | 2
Deformation | Bs | {011}<211> | 35 | 45 | 0
 | S | {123}<634> | 55 | 35 | 65
 | Cu | {112}<111> | 90 | 30 | 45
 | Shear1 | {001}<110> | 0 | 0 | 45
 | Shear2 | {111}<110> | 0 | 55 | 45
 | Shear3 | {112}<110> | 0 | 35 | 45
Recrystallization | Goss | {011}<001> | 0 | 45 | 0
 | Cube | {001}<100> | 0 | 0 | 0
 | RCRD1 | {013}<100> | 0 | 20 | 0
 | RCRD2 | {023}<100> | 0 | 35 | 0
 | RCND1 | {001}<310> | 20 | 0 | 0
 | RCND2 | {001}<320> | 35 | 0 | 0
 | P | {011}<122> | 70 | 45 | 0
 | Q | {013}<231> | 55 | 20 | 0
 | R | {124}<211> | 55 | 75 | 25

## Slide 29
fcc/ bcc/ hcp (Ti)
Shear: A:{111}<uvw> E:{110}<001> ? B:{hkl}<110> D:{112}<110>
C: {001}<110>
Rolling: Partial Fibers:
beta, alpha gamma, alpha {0001} split to +/-TD

## Slide 30: Fcc rolling textures
The next set of slides summarizes rolling textures in fcc metals. This topic was also presented as an example in the discussion of Orientation Distributions and their graphical representation.

## Slide 32: Cartesian Euler Space
f1
F
f2

## Slide 33: Sections
f2 = 0°
f2 = 5°
f2 = 15°
f2 = 10°
f1
F
f2

## Slide 34
PF Representation
Note how very different components tend to overlap in a pole figure.

## Slide 35
Fiber Plots: various rolling reductions:
(a) intensity versus
position along the fiber (b) angular position of intensity maximum versus position along the fiber
Kocks, Ch. 2
b-fiber

## Slide 36: Volume fraction vs. density (intensity)
• Volume fraction associated with region around the fiber in a given section.
• Vf increases faster than density with increasing F. • Location of max. density not at nominal location.
Kocks, Tomé, Wenk: Ch. 2

## Slide 37: Rolling fcc Cu: Effect of Strain
von Mises strains= initial, 0.5, 1.0, 2.0, 2.7, 3.5
{111} Pole Figures, RD vertical

## Slide 38: Effect of Alloying: Cu-Zn (brass); the texture transition
Zn content: (a) 0%, (b) 2.5%, (c) 5%, (d) 10%, (e) 20% and (f) 30% [Stephens PhD, U Arizona, 1968]
Copper component
Brass

## Slide 39: Alloy, Precipitation Effects
Hirsch & Lücke, 1988 , Acta metall. 36, 2863
Engler et al., 1989, Acta metall. 37, 2743
copper
copper
brass
brass

## Slide 40: Rolling Textures BCC
{110} and {100} pole figures (equal area projection; rolling direction vertical) for (a) low-carbon steel cold rolled to a reduction in thickness of 80% (approximate equivalent strain of 2); (b) tantalum, unidirectionally rolled at room temperature to a reduction in thickness of 91%.
Kocks, Ch. 5

## Slide 41: {100} Pole figure for certain components of rolled BCC metals
Note how very different components tend to overlap in a pole figure.
Kocks, Ch. 5
Notes: Pole figures are evidently less than ideal for distinguishing particular components!

## Slide 42: BCC fibers: the f2 = 45° section
g, <111>||ND
a,
<110>||RD
e, <110>||TD
Goss
F
f1

## Slide 43: Ta, Fe rolling textures
Note: Euler angles are Roe angles: axes transposed with Q horiz., y vertical.

## Slide 44: Fe, Fe-Si rolling fiber plots
Note the marked alloy dependence in the alpha fiber; smaller variations in the gamma fiber.

## Slide 45: Summary: part 1
Typical textures illustrated for FCC & BCC metals as a function of alloy type (stacking fault energy) and deformation character (strain type).
Pole figures are recognizable for standard deformation histories but orientation distributions provide much more detailed information. Inverse pole figures are also useful, especially for uniaxial textures.
Measure strain using von Mises equivalent strain.
Plane strain (rolling) textures concentrate on characteristic lines ("partial fibers") in orientation space.
Uniaxial textures align certain crystal axes with the deformation axis.

## Slide 46: Part 2: shear/ torsion textures
This section covers shear (torsion) textures

## Slide 47: Shear Texture
Shear strain means that displacements are tangential to the direction in which they increase.
Shear direction=1, Shear Plane  2-axis
The matrix shows the velocity gradient; the strain (rate) is the symmetrized version of L.
e12= tanq
1 = Shear Direction = <uvw>
2 = Torsion Axis = {hkl}
Note the definition of strain, eij, as the derivative of the displacement ui with respect to coordinate xj.
q

## Slide 48: Torsion Textures: twisting of a hollow cylinder specimen
(a)
(b)
(c)
Torsion Axis
Sense of shear:

## Slide 49: Shear Textures: idealized texture components for FCC metals
Torsion Axis
Shear direction
C component: {001}<110>
B partial fiber {hkl}<110>
A partial fiber {111}<uvw>
Canova et al. (1982), 'Texture Development Prediction for Deformation in Torsion and Tension at Large Strains', J. Metals 35 A21-A21; Canova et al. (1984), 'Theory of Torsion Texture Development', Acta metall. 32 211

## Slide 50: FCC Torsion Textures
  Plots of {111} and {200} pole figures (equal area projection; torsion axis vertical) for the following materials deformed in torsion; the shear direction points to the left in these figures.
  a) Nickel at g=3.6
  b) Copper at g=3.5
  c) Silver at g=3.5
  d) Cu-30Zn at g=3.5
  e) Ni-60Co at g=3.2
Note that the partial "A" fiber is present in Ni and Cu, but is absent in the other materials. Silver, brass and Ni-60Co show instead a "D" fiber which is similar to the A fiber but rotated approximately 90° about the torsion axis. The B fiber is present to varying degrees in all the materials.
Kocks, Ch. 5

## Slide 51: Shear Texture Components
Why study shear textures? Shear strain is common near the surface of rolled parts, for example.
Partial Fibers: A/D {111}<uvw>…<110> B {hkl}<110> … {112} Components C {001}<110> D {112}<111> E {011}<111> F {110}<001>

## Slide 52: FCC vs. BCC {100} Pole figures
FCC
BCC
Montheillet et al. (1985), Acta metall., 33 705

## Slide 53: BCC torsion textures: Fe
Ideal |{100} pole figures

## Slide 54: BCC torsion textures: Ta
(a) initial texture from swaged rod;
(b) torsion texture
Ideal |{100} pole figures
Kocks, Ch. 5

## Slide 55: Hexagonal Metals
Common to show the (0001) pole figure: provides most information needed.
Easy slip on the basal plane means that compression generally aligns the basal plane normal with the compression axis.
Tension typically aligns basal plane normals perpendicular to the axis.

## Slide 56: Deformation systems, hexagonal
Acta mater. 49 (2001) 3085–3096

## Slide 57: Uniaxial textures in Ti
Compression: 25° from 0001,
~ <11-24>
compression
tension
Kocks, Ch. 5

## Slide 58: Zr: compression Ti: compression
Kocks, Ch. 5

## Slide 59: Hexagonal Rolling Textures; schematic
c/a > 1.633: RD split in 0001
c/a < 1.633:
TD split in 0001
Kocks, Ch. 5

## Slide 60: Hexagonal Rolling Textures: exptl.
Kocks, Ch. 5

## Slide 61: Hexagonal Rolling: strain dependence
20%
30%
55%
97%
Kocks, Ch. 5

## Slide 62: Hexagonal: clock rolling
Tomé et al. (2001) Acta mater. 49 3085–3096
Note the strong anisotropy caused by texture