## Slide 1: Thermomechanical Processing Textures, part 3
Updated 26th Apr. 2014
A. D. Rollett
27-750 Texture, Microstructure & Anisotropy

## Slide 2: Objective
Part 3 of the notes on typical textures covers solidification textures and textures in hexagonal metals and composites.

## Slide 3: Solidification texture: <100> growth directions

## Slide 4: Melt-spun Palladium columnar structures

## Slide 5: Hexagonal Metals
Common to show the (0001) pole figure: provides most information needed.
Easy slip on the basal plane means that compression generally aligns the basal plane normal with the compression axis.
Tension typically aligns basal plane normals perpendicular to the axis.

## Slide 6: Uniaxial textures in Ti
Compression: 25° from 0001,
~ <11-24>
compression
tension

## Slide 7: Zr: compression Ti: compression

## Slide 8: hcp Rolling Textures; schematic
c/a > 1.633: RD split in 0001
c/a < 1.633:
TD split in 0001
Kocks, Ch. 5

## Slide 9: hcp Rolling Textures: exptl.
Kocks, Ch. 5

## Slide 10: hcp: Rolling: strain dependence
20%
30%
55%
97%
Kocks, Ch. 5

## Slide 11: Al-SiC composites
• Reinforcement tends to randomize texture
Kocks, Ch. 5

## Slide 12: Al-SiC: Fibers vs. particles:
• Randomization from particles less than for fibers
Kocks, Ch. 5

## Slide 13: Summary: part 3
Typical textures illustrated for solidification, metal matrix composites and for deformed hexagonal metals.
Solidification textures can be strong but are often ignored in processing histories!
Significant alloy dependence observed in hexagonal metals.
Composites generally have weaker textures than equivalently deformed single phase metals.