## Slide 1: Typical Textures, part 2 FCC Torsion, BCC textures
A. D. Rollett
27-750 Texture, Microstructure & Anisotropy
Last revised: 26th Apr. ‘14

## Slide 2: Objectives
Part 1 of the slides covers shear (torsion) and rolling textures; part 2 covers some aspects of textures in BCC metals.

## Slide 3: Shear Texture
Shear strain means that displacements are tangential to the direction in which they increase.
Shear direction=1, Shear Plane  2-axis
e12= tanq
1 = Shear Direction = <uvw>
2 = Torsion Axis = {hkl}
Note the definition of strain, eij, as the derivative of the displacement ui with respect to coordinate xj.
q

## Slide 4: Torsion Textures: twisting of a hollow cylinder specimen
(a)
(b)
(c)
Torsion Axis
Sense of shear:

## Slide 5: Shear Textures: idealized texture components for FCC metals
Torsion Axis
Shear direction
C component: {001}<110>
B partial fiber {hkl}<110>
A partial fiber {111}<uvw>

## Slide 6: Shear Texture Components
Why study shear textures? Shear strain is common near the surface of rolled parts, for example.
Partial Fibers: A/D {111}<uvw>…<110> B {hkl}<110> … {112} Components C {001}<110> D {112}<111> E {011}<111> F {110}<001>

## Slide 7: {100} Pole figures Montheillet et al., Acta metall., 33, 705, 1985
FCC
BCC

## Slide 8: FCC Torsion Textures
  Plots of {111} and {200} pole figures (equal area projection; torsion axis vertical) for the following materials deformed in torsion; the shear direction points to the left in these figures.
  a) Nickel at g=3.6
  b) Copper at g=3.5
  c) Silver at g=3.5
  d) Cu-30Zn at g=3.5
  e) Ni-60Co at g=3.2
Note that the partial "A" fiber is present in Ni and Cu, but is absent in the other materials. Silver, brass and Ni-60Co show instead a "D" fiber which is similar to the A fiber but rotated approximately 90° about the torsion axis. The B fiber is present to varying degrees in all the materials.
Kocks, Ch. 5

## Slide 9: BCC uniaxial textures
92% rolled Ta Tensile test in original RD to strain of 0.6: <110> fiber
(a) Normal and rolling direction inverse pole figures (equal area projection) of 92% rolled Ta and (b) Prior normal and rolling direction inverse pole figures for (a) tested in tension to a strain of 0.6 (tensile direction coincident to prior rolling direction).
Kocks, Ch. 5

## Slide 10: BCC torsion textures: Fe
Ideal |{100} pole figures

## Slide 11: BCC torsion textures: Ta
(a) initial texture from swaged rod;
(b) torsion texture
Ideal |{100} pole figures
Kocks, Ch. 5

## Slide 12: Rolling Textures BCC
{110} and {100} pole figures (equal area projection; rolling direction vertical) for (a) low-carbon steel cold rolled to a reduction in thickness of 80% (approximate equivalent strain of 2); (b) tantalum, unidirectionally rolled at room temperature to a reduction in thickness of 91%.
Kocks, Ch. 5

## Slide 13: {100} Pole figure for certain components of rolled BCC metals
Note how very different components tend to overlap in a pole figure.
Kocks, Ch. 5
Notes: Pole figures are evidently less than ideal for distinguishing particular components!

## Slide 14: BCC fibers: the f2 = 45° section
g, <111>||ND
a,
<110>||RD
e, <110>||TD
Goss
F
f1

## Slide 15: Ta,Fe rolling textures
Note: Euler angles are Roe angles: axes transposed with Q horiz., y vertical.

## Slide 16: Fe,Fe-Si rolling fiber plots
Note the marked alloy dependence in the alpha fiber; smaller variations in the gamma fiber.

## Slide 17: Summary: part 2
Typical textures illustrated for shear textures and for bcc metals.
Pole figures are recognizable for standard deformation histories but orientation distributions provide much more detailed information.