## Slide 1
Typical Textures, part 1: Thermomechanical Processing (TMP) of Metals
Last revised: 26th Apr. 2014
A. D. Rollett
27-750 Texture, Microstructure & Anisotropy

## Slide 2: Objectives
Introduce you to experimentally observed textures in a wide range of materials.
Develop a taxonomy of textures based on deformation type.
Prepare you for relating observed textures to theoretical (numerical) models of texture development, especially the Taylor model.
See chapter 5 in Kocks, Tomé & Wenk.
Some slides courtesy of Prof. P. Kalu (FAMU) and Prof. D. Waryoba (Penn State Dubois)

## Slide 3: Taxonomy
Deformation history more significant than alloy.
Crystal structure determines texture through slip (and twinning) characteristics.
Alloy (and temperature) can affect textures through planarity of slip.
Annealing (recrystallization) sometimes produces a drastic change in texture.

## Slide 4: Why does deformation result in texture development?
Qualitative discussion:
Deformation means that a body changes its shape, which is quantified by the plastic strain, ep.
Plastic strain is accommodated in crystalline materials by dislocation motion, or by re-alignment of long chain molecules in polymers.

## Slide 5: Dislocation glide ⇒ grain reorientation
Dislocation motion at low (homologous) temperatures occurs by glide of loops on crystallographic planes in crystallographic directions: restricted glide.
Restricted glide throughout the volume is equivalent to uniform shear.
In general, shear requires lattice rotation in order to maintain grain alignment: compatibility

## Slide 6: Re-orientation  Preferred orientation
Reorientations experienced by grains depend on the type of strain (compression versus rolling, e.g.) and the type of slip (e.g. {111}<110> in fcc).
In general, some orientations are unstable (f(g) decreases) and some are stable (f(g) increases) with respect to the deformation imposed, hence texture development.

## Slide 7: The Taylor model
The Taylor model has one basic assumption: the change in shape (micro-strain) of each grain is identical to the body’s change in shape (macro-strain).
Named for G.I. Taylor, English physicist, mid-20th century; first to provide a quantitative explanation of texture development.

## Slide 8: Single slip models ineffective
Elementary approach to single crystal deformation emphasizes slip on a single deformation system.
Polycrystal texture development requires multiple slip systems (5 or more, as dictated by von Mises).
Cannot use simple rules, e.g. alignment of slip plane with compression plane!

## Slide 9: Deformation systems (typical)
Fcc metals (low temperature): {111}<110>
Bcc metals: {110}<111>, {112}<111>, {123}<111>, pencil glide
Hexagonal metals: {1010}<1210>; {0001}<1210>; {1012}<1011>twin; {1011}<1123>; {2112}<2113>twin.

## Slide 10: Deformation systems (typical)
In deformed materials, texture or preferred orientation exists due to the anisotropy of slip. While slip in bcc metals generally occurs in the <111> type direction, it may be restricted to {110} planes or it may involve other planes (T. H. Courtney, Mechanical Behavior of Materials, McGraw-Hill, New York, 1990.)

## Slide 11: Strain Measures
Strain commonly defined as a scalar measure of (plastic, irreversible) deformation: logarithmic strain:= e = ln {lnew/lold}
Rolling strain: typical: reduction in thickness:= r = 100% x hnew/hold better (!) = von Mises equivalent strain evM = 2/√3 ln {lold/lnew}

## Slide 12: Deformation Modes: sample symmetry
Tension, Wire Drawing, Extrusion C
Compression, Upsetting C
Torsion, Shear 2
Plane Strain Compression, Rolling mmm
Deformation modes of uniaxial type generate fiber textures
Shear gives monoclinic symmetry
Plane strain gives orthorhombic symmetry

## Slide 13: Axisymmetric deformation: Extrusion, Drawing

## Slide 14: Uniaxial Strain
tension
compression
C
Inverse Pole Figures (FCC)

## Slide 15: Uniaxial Modes - C
Deformation mode/ fcc/ bcc/ hcp (Ti)
Wire drawing, <111> <110> <10-10>
Round extrusion. & <100>
Upsetting, <110> <111> <0001>
Uniaxial compression. &<100>
Note exchange of types between fcc & bcc

## Slide 16
In fcc metals, axisymmetric deformation (e.g. wire drawing) produces fiber texture: <111> + <100> duplex, parallel to the wire.
Schmid and Wassermann (1963): 60% <111> + 40% <100>
Ahlborn and Wassermann (1963): 66% <111> + 34% <100>
Electrolytic Copper
}
McHargue et al., 1959
Axisymmetric deformation

## Slide 17
Axisymmetric deformation
Axisymmetric deformation ~ higher order symmetry, C
Texture can be represented by an inverse pole figure (IPF).
In IPF, contour lines show the frequency with which the various directions, <uvw>, in the crystal coincide with the specimen axis under consideration
DD
TD
ND
DD – Drawing direction corresponds to RD in rolling

## Slide 18
The relative proportions of the two components are determined by the stacking fault energy [English et al., 1965] and vary in a complex manner.
Axisymmetric deformation

## Slide 19
Effect of deformation strain
001
101
111
001
101
111
001
101
111
Max = 6.9
Max = 7.7
Max = 5.3
 = 2.80
 = 3.10
 = 3.56
001
101
111
001
101
111
001
101
111
111
001
101
Max = 4.1
Max = 4.5
Max = 5.0
Max = 5.4
 = 0.0
 = 0.45
 = 1.29
 = 2.31
D. R. Waryoba, Ph. D. Dissertation, FSU, 2003
X-ray IPFs showing the effect of strain on the texture of OFHC copper wire

## Slide 20
Max. = 5.29
Max. = 6.85
Max. = 2.06
Max. = 2.10
Max. = 2.48
Max. = 2.44
Max. = 4.65
Max. = 5.97
RT
180°C
250°C
300°C
450°C
500°C
600°C
750°C
X-ray IPFs showing the effect of annealing temperature on the texture of OFHC copper wire, initially drawn to true strain of 2.31
D. R. Waryoba and P. N. Kalu, TMS 2003,San Diego, CA
Effect of Temperature

## Slide 21: Uniaxial Compression: fcc
Initial texture theoretical texture exptl. texture
[Kocks Ch. 5: Inverse Pole Figures]

## Slide 22
Texture inhomogeneity in Drawn Wires
III
II
I
Max = 4.2
Max = 3.5
Max = 15.7
OIM IPFs representing outer region, mid region, and inner core of the OFHC Cu wire drawn to true strain of 2.31 (contours are at 1, 2, 3 … times random)
D. R. Waryoba and P. N. Kalu, TMS 2005, San Francisco, CA

## Slide 23
Max = 9.2
Max = 5.3
Max = 5.1
10 min
OIM IPFs representing outer region, mid region, and inner core of the OFHC Cu wire drawn to true strain of 2.31 and annealed at 250°C for 10 min (contours are at 1, 2, 3 … times random)
Texture inhomogeneity in Drawn Wires
D. R. Waryoba and P. N. Kalu, TMS 2005, San Francisco, CA

## Slide 24: Rolling = Plane Strain
RD
ND
Rolling ~ plane strain deformation means extension or compression in a pair of directions with zero strain in the third direction: a multiaxial strain.

## Slide 25: Plane strain (rolling)
Plane strain means extension/compression in a pair of directions with zero strain in the third direction: a multiaxial strain.
tension
compression
3
1

## Slide 26: Typical rolling texture in FCC Materials
Type | Component | {hkl}<uvw> | Euler Angles (Bunge) |  | 
 |  |  | 1 |  | 2
Deformation | Bs | {011}<211> | 35 | 45 | 0
 | S | {123}<634> | 55 | 35 | 65
 | Cu | {112}<111> | 90 | 30 | 45
 | Shear1 | {001}<110> | 0 | 0 | 45
 | Shear2 | {111}<110> | 0 | 55 | 45
 | Shear3 | {112}<110> | 0 | 35 | 45
Recrystallization | Goss | {011}<001> | 0 | 45 | 0
 | Cube | {001}<100> | 0 | 0 | 0
 | RCRD1 | {013}<100> | 0 | 20 | 0
 | RCRD2 | {023}<100> | 0 | 35 | 0
 | RCND1 | {001}<310> | 20 | 0 | 0
 | RCND2 | {001}<320> | 35 | 0 | 0
 | P | {011}<122> | 70 | 45 | 0
 | Q | {013}<231> | 55 | 20 | 0
 | R | {124}<211> | 55 | 75 | 25

## Slide 27
fcc/ bcc/ hcp (Ti)
Shear: A:{111}<uvw> E:{110}<001> ?? B:{hkl}<110> D:{112}<110>
C: {001}<110>
Rolling: Partial Fibers:
beta, alpha gamma, alpha {0001}

## Slide 29: Cartesian Euler Space
f1
F
f2

## Slide 30: Sections
f2 = 0°
f2 = 5°
f2 = 15°
f2 = 10°
f1
F
f2

## Slide 31
PF Representation
Note how very different components tend to overlap in a pole figure.

## Slide 32
Fiber Plots: various rolling reductions:
(a) intensity versus
position along the fiber (b) angular position of intensity maximum versus position along the fiber
Kocks, Ch. 2
b-fiber

## Slide 33: Volume fraction vs. density (intensity)
• Volume fraction associated with region around the fiber in a given section.
• Vf increases faster than density with increasing F. • Location of max. density not at nominal location.
Kocks, Ch. 2

## Slide 34: Rolling fcc Cu: Effect of Strain
von Mises strains= initial, 0.5, 1.0, 2.0, 2.7, 3.5
{111} Pole Figures, RD vertical

## Slide 35: Effect of Alloying: Cu-Zn (brass); the texture transition
Zn content: (a) 0%, (b) 2.5%, (c) 5%, (d) 10%, (e) 20% and (f) 30% [Stephens PhD, U Arizona, 1968]
Copper component
Brass

## Slide 36: Alloy, Precipitation Effects
Hirsch & Lücke, 1988 , Acta metall. 36, 2863
Engler et al., 1989, Acta metall. 37, 2743
copper
copper
brass
brass

## Slide 37: Summary: part 1
Typical textures illustrated for FCC metals as a function of alloy type (stacking fault energy) and deformation character (strain type).
Pole figures are recognizable for standard deformation histories but orientation distributions provide much more detailed information. Inverse pole figures are also useful, especially for uniaxial textures.
Measure strain using von Mises equivalent strain.
Plane strain (rolling) textures concentrate on characteristic lines ("partial fibers") in orientation space.
Uniaxial textures align certain crystal axes with the deformation axis.