## Slide 1: Polycrystal Plasticity - Self-Consistent Model
27-731 (normally, 27-750)
Texture, Microstructure & Anisotropy
A.D. Rollett, J.V. Gordon
  Lecture notes originally by: Carlos Tomé (LANL) Hamid Garmestani (GaTech), Gilberto Branco (FAMU/FSU)
Last revised: 17th October, 2020

## Slide 2: Objective
The objective of this lecture is to explain how we can use Eshelby's theory of interaction between an inclusion and its surrounding matrix to model anisotropic deformation.
Further, to show how to calculate the stresses and distribution of slips in each grain of a polycrystal using the Viscoplastic Selfconsistent code, VPSC.
A basic understanding of how polycrystal plasticity works based on multiple slip in each grain.
Requirements:

## Slide 3: Questions & Answers

## Slide 4: References
Key Paper: Lebensohn RA and Tome CN (1993) "A Self-Consistent Anisotropic Approach for the Simulation of Plastic-Deformation and Texture Development of Polycrystals - Application to Zirconium Alloys" Acta Metall. Mater. 41 2611-2624.
Taylor G (1938) "Plastic strain in metals", J. Inst. Metals (U.K.) 62 307 ; Bishop J and Hill R (1951), Phil. Mag. 42 1298; Van Houtte P (1988), Textures and Microstructures 8 & 9 313-350; Kocks, Tomé & Wenk: Texture & Anisotropy (Cambridge); chapter 8, 1996. Detailed analysis of plastic deformation and texture development.
Reid: Deformation Geometry for Materials Scientists, 1973. Older text with many nice worked examples. Be careful of his examples of calculation of Taylor factor because, like Bunge & others, he does not use von Mises equivalent stress/strain to obtain a scalar value from a multiaxial stress/strain state.
Hosford: The Mechanics of Crystals and Textured Polycrystals, Oxford, 1993. Written from the perspective of a mechanical metallurgist with decades of experimental and analytical experience in the area.
Khan & Huang: Continuum Theory of Plasticity, Wiley-Interscience, 1995. Written from the perspective of continuum mechanics.
De Souza Neto, Peric & Owen: Computational Methods for Plasticity, 2008 (Wiley). Written from the perspective of continuum mechanics.
Gurtin: An Introduction to Continuum Mechanics, ISBN 0123097509, Academic Press, 1981.

## Slide 5: Background, Concepts

## Slide 6: Eigenstrains and Eigenstresses
Thermal Expansion
Replace
region
and remove
surface tractions
Remove
region
Apply surface
tractions
Transforming region
Non-transforming
matrix
Eigenstresses result!
Eigenstrains result!
Notes: First we start with a transforming region (or inclusion) inside a non-transforming matrix. If we allow the inclusion to undergo some kind of transformation which can be a phase transformation, thermal expansion, or any other volume changing transformation where no stress is applied free of the matrix. For this explanation we will assume it is a volume expansion. The resulting strains are called eigenstrains. Now, if we apply surface tractions to counteract the volume change caused by the eigenstrains so that the inclusion returns to it’s original size, we can replace the region inside the non-transforming matrix easily/nicely. Finally we remove the surface tractions and the matrix will constrain the expansion of the inclusion – the inclusion will not return to it’s free expansion volume. This will cause stresses inside of the body. Because these stresses were formed by eigenstrains, they are called eigenstresses.
Not sure if I should use this or not:
It is important to not that these eigenstrains are result from a transformation but not when a stress is applied. These types of strains are called elastic strains. How to include the equations?

## Slide 7: Self-Consistent Model
Following slides contain information about a more sophisticated model for crystal plasticity, called the self-consistent model.
It is based on a finding a mean-field approximation to the environment of each individual grain.
This provides the basis for the popular code VPSC made available by Tomé and Lebensohn (Lebensohn, R. A. and C. N. Tome (1993). "A Self-Consistent Anisotropic Approach for the Simulation of Plastic-Deformation and Texture Development of Polycrystals - Application to Zirconium Alloys." Acta Metallurgica et Materialia 41 2611-2624).

## Slide 8: VPSC: Inclusion

## Slide 9: Eshelby Theory
Eshelby analyzed the situation of an ellipsoidal inclusion within an infinite matrix that has undergone some eigenstrain. A thermoelastic potential may be defined for inclusions in a matrix with thermal eigen- strains and used to compute the resultant thermal stresses. The potential is employed to determine the displacement at all locations within the solid. Eshelby used this formulation to compute surface integrals at the inclusion surface, which he later simplified to what are known today as Eshelby tensors. These Eshelby tensors transform the local thermoelastic eigenstrain tensors to local total strain tensors.
One of the most significant conclusions from Eshelby’s approach is the finding that surface integrals are independent of location within the inclusion itself, and thus, the stress and strain states are constant. For spherical symmetry, the 3 independent tensors are computed as shown on the right.

## Slide 10
Kröner, Budiansky and Wu’s Model
Taylor Model
- compatibility across grain boundary
- violation of the equilibrium between the grains
Budiansky and Wu’s Model
- Self-consistent model
- Ensures both compatibility and equilibrium conditions on grain boundaries - Based on the Eshelby inclusion model

## Slide 11
Kröner, Budiansky and Wu’s Model
The model:
Sphere (single crystal grain) embedded in a homogeneous polycrystal matrix.
Can be described by an elastic stiffness tensor C, which has an inverse C-1.
The matrix is considered to be of infinite extent.
The overall quantities and are considered to be the average values of the local quantities and over all randomly distributed single crystal grains.
The grain and the matrix are elastically isotropic.
Khan & Huang

## Slide 12
Kröner, Budiansky and Wu’s Model
The initial problem can be solved by the following approach
1 – split the proposed scheme into two others as follows
Khan & Huang

## Slide 13
Kröner, Budiansky and Wu’s Model
1.a – The aggregate and grain are subject to the overall quantities and . In this case the total strain is given by the sum of the elastic and plastic strains:
Khan & Huang

## Slide 14
Kröner, Budiansky and Wu’s Model
1.b – The sphere
has a stress-free transformation strain, e’, which originates in the difference in plastic response of the individual grain from the matrix as a whole. This transformation strain is an eigenstrain.
has the same elastic property as the aggregate.
is small when compared with the aggregate (the aggregate is considered to extend to infinity).
Notes: Consider the “stress-free transformation strain” to be the same as an EIGENSTRAIN. Where this comes from is the difference in plastic behavior between the grain itself and the matrix.

## Slide 15
Kröner, Budiansky and Wu’s Model
The strain inside the sphere due to the elastic interaction between the grain and the aggregate caused by is given by
Where,
S is the Eshelby tensor (not a compliance tensor) for a spherical inclusion in an isotropic elastic matrix

## Slide 16
Kröner, Budiansky and Wu’s Model
Then the actual strain inside the sphere is given by the sum of the two representations (1a and 1b) as follows
Given that,
where
This leads to
The fraction was shown earlier as S1212

## Slide 17
Kröner, Budiansky and Wu’s Model
From the previous equation, it follows that the stress inside the sphere is given by

## Slide 18
Kröner, Budiansky and Wu’s Model
In incremental form
where

## Slide 19: ViscoPlastic-SelfConsistent code (VPSC)
VPSC is based on the Taylor model (uniform plastic strain across a polycrystal) but modified to allow for interactions between each grain and the polycrystal in which it is embedded.
There is no microstructure in VPSC: it works with just a set (list) of orientations. Therefore there is no local interaction between a grain and some set of neighbor grains, only with the homogeneous effective medium (HEM).
The modification allows the deformation of each grain to deviate from that of the polycrystal. The constraint on each grain is computed with Eshelby theory (for inclusions).
Compared to any FE or FFT computation with crystal plasticity, VPSC is an order of magnitude more efficient. For example, it is very useful for fitting Voce hardening parameters to experimental data. It is also very efficient for determining constitutive parameters such as CRSS values for fitting to experimental texture data.

## Slide 20: VPSC
Source: Carlos Tome, EFRC Summer School 2012
Each grain is a visco-plastic anisotropic ellipsoidal inclusion embedded in a visco-plastic anisotropic Homogeneous Effective Medium (HEM).
Eshelby result: Stress and strain rate are uniform inside the inclusion but differ from macroscopic (average) values
Interaction between stress in inclusion with average stress
Avg stress= Macroscopic stress -> Self consistent

## Slide 21: Assumptions for VPSC
Kocks, Tomé, Wenk

## Slide 22: FULL CONSTRAINTS (FC) POLYCRYSTAL MODEL
Also known as Taylor model. Based on enforcing strain continuity over stress equilibrium. Represents an absolute upper bound for macroscopic stress.
grain strain rate
impose
Imposes the same velocity gradient (plastic strain and plastic spin) to all the grains
solve non-linear equation (typically n=20) for the stress in each grain
calculate shear rates in every slip system
update hardening and grain orientation incrementally

## Slide 23: VISCO-PLASTIC SELF-CONSISTENT (VPSC) POLYCRYSTAL MODEL [1]
Each grain is a visco-plastic anisotropic ellipsoidal inclusion embedded in a visco-plastic anisotropic Homogeneous Effective Medium (HEM).
Deviatoric constitutive response:
grain
medium
[1] R.A. Lebensohn & C.N. Tomé, Acta Materialia 41 (1993) 2611
b
n
Solve stress equilibrium equation for inclusion in the homogeneous medium
Eshelby result: stress and strain-rate are uniform inside the inclusion …but different from the macroscopic stress and strain rate !

## Slide 24: VPSC model  interaction equation
M is the compliance of the medium and relates stress with strain rate
Solving stress equilibrium equation for the VP inclusion embedded in the VP medium leads to the interaction equation
M large: the medium is very compliant  stress continuity  Sachs
M small: the medium is very stiff  strain continuity  Taylor
Intermediate cases: secant, affine, tangent
affine

## Slide 25: Visco-Plastic Self-Consistent Polycrystal Model
B: localization tensor
Assumption for having a polycrystal model: treat each grain as an inclusion inside the effective macroscopic medium.
The condition that the average stress over all grains has to be equal to the macroscopic stress …
…leads to a self-consistent equation for the plastic moduli of the aggregate:
The interaction equation can be written as a localization equation that relates stress in the inclusion with average stress

## Slide 26: Hardening of slip modes inside VPSC
An ‘extended Voce’ law is used in VPSC to describe the hardening of slip and twin systems vs accumulated shear in grain 
0.0
-0.1
-0.2
-0.3
-0.4
-0.5
0
100
200
300
400
s
ND
[MPa]
AA5182 measured
AA5182 predicted
e
ND
If latent hardening parameters h are considered the CRSS is incrementally updated as:
else:

## Slide 27: Running the code VPSC: input & output
INPUT:
Parameters of the run and names of datafiles (file VPSC7.IN)
  INITIAL TEXTURE (discrete orientation file)
  ACTIVE SLIP AND TWIN SYSTEMS (hardening parameters)
  MACROSCOPIC VELOCITY GRADIENT (strain history)
OUTPUT:
Parameters of the run and input data (file RUN_LOG.OUT)
  FINAL TEXTURE (discrete orientation file  TEX_PH1.OUT)
  STRESS-STRAIN RESPONSE (hardening  STR_STR.OUT)
  STATISTICS (system activity, twin fractions  ACT_PH1.OUT)

## Slide 28: Running VPSC  control file VPSC7.IN
. . . . . .
0 grain shape and orient ctrl (ishape=0 to 4)
1.0 1.0 1.0 initial ellipsoid ratios (dummy if ishape=4)
0.0 0.0 0.0 init Eul ang ellips axes (dummy if ishape=3,4)
* name and path of texture file (filetext)
example1\rand500.tex
* name and path of single crystal file (filecrys)
example1\fcc.sx
. . . . . . .
. . . . . . .
*MODELING CONDITIONS FOR THE RUN
0 ihardlaw (0:Voce, 1:MTS, 2:composite grain)
1 iratesens (0:rate insensitive, 1:rate sensitive)
0 interaction (0:FC,1:affine,2:secant,3:neff=10,4:tangent,5:SO)
1 1 1 iupdate: update orient, grain shape, hardening
. . . . . .
*NUMBER OF PROCESSES
1
*IVGVAR AND PATH\NAME OF FILE FOR EACH PROCESS
0
example1\tension.3

## Slide 29: Running VPSC7  TEXTURE file
dummy
dummy
random texture generated by RANDTEXT.FOR (23/01/97)
B 500
102.74 119.56 33.65 1.000000
219.06 36.21 70.51 1.000000
166.66 28.59 45.80 1.000000
149.74 86.13 38.68 1.000000
. . . . . . .
. . . . . . .
RAND500.TEX  a file containing 500 randomly generated orientations

## Slide 30: Running VPSC7  PROCESS file
50 3 0.02 298. nsteps ictrl eqincr temp
* boundary conditions
1 1 1 iudot | flag for vel.grad.
1 1 1 | (0:unkn-1:known)
1 1 1 |
-0.5 0. 0. udot | vel.grad
0. -0.5 0. |
0. 0. 1.0 |
0 0 0 iscau | flag for Cauchy
0 0 | (0:unkn-1:known)
0 |
0. 0. 0. scauchy | Cauchy stress
0. 0. |
0. |
TENSION.3  50 steps of 2% axial strain along direction 3

## Slide 31: Running VPSC7  SINGLE CRYSTAL FILE
*Material: AUSTENITIC STEEL
cubic crysym
1. 1. 1. 90. 90. 90. unit cell axes and angles
Elastic stiffness (single crystal [GPa])
205.0 138.0 138.0 000.0 000.0 000.0
….
*Info about slip & twinning modes in this file:
2 nmodesx (total # of modes listed in file)
1 nmodes (# of modes to be used in the calculation)
1 mode(i) (label of the modes to be used)
<111>{110} SLIP
1 12 20 1 modex,nsmx,nrsx,iopsysx
0.000 0 0.000 0.000 twshx,isectw,thres1,thres2
1.0 0.0 0.0 0.0 0. 0. tau0,tau1,thet0,thet1 ,hpfac,gndfac
1.0 1.0 hlat(nmodes)
1 1 1 0 1 -1
1 1 1 1 0 -1
1 1 1 1 -1 0
………. ………
FCC.SX  slip systems and hardening parameters for FCC

## Slide 32: EXAMPLE 1: TENSION & COMPRESSION of FCC
Simulate axial tension and compression of an initially random FCC aggregate.
Deformation by slip in the <110> direction and on {111} crystallographic planes. The CRSS = ts = constant = 1
The Voce hardening is rigid perfectly plastic:
The imposed velocity gradient is symmetric and equal to the strain rate tensor:

## Slide 33: EXAMPLE 1: TENSION & COMPRESSION of FCC  TEXTURE
Predicted textures after 100% axial tension and compression using different grain-matrix interaction and compression (INTERACTION=0,1,2,3,4)
TENSION
COMPRESSION

## Slide 34: EXAMPLE 1: TENSION & COMPRESSION of FCC  STRESS
Stress (Taylor factor) evolution and Average Number of Active Systems per Grain using different grain-matrix interaction assumptions.
TAYLOR (FC):
upper bound and more than 6 active systems
TANGENT:
lower bound, about 4 active systems in tension and 3 in compression.
In general: Self-Consistent leads to plane strain deformation of individual grains

## Slide 35: EXAMPLE 2: ROLLING of FCC
Simulate plane strain deformation of an initially random FCC aggregate.
Deformation by slip in the <110> direction and on {111} crystallographic planes, up to E33=100% (63% reduction).
The Voce hardening is linearly increasing:
The imposed velocity gradient is plane strain (EXAMPLE 2a):
We also run plane strain with superimposed shear (EXAMPLE 2b):

## Slide 36: EXAMPLE 2: ROLLING of FCC  PROCESS FILE
File VPSC7.INa enforces rolling followed by a yield locus calculation and a Lankford and Young modulus calculation.
. . . . . .
. . . . . .
*NUMBER OF PROCESSES
3
*IVGVAR AND PATH\NAME OF FILE OR STRESS SUBSPACE OR ANG INCREM
0 ivgvar=0 will run a monotonic strain path
example2\rolling
2 ivgvar=2 will calculate PCYS at the end
1 2 --> section of stress space
3 ivgvar=3 will calculate Lankford coefficients at the end
10 --> angular increment for tensile probing

## Slide 37: EXAMPLE 2: ROLLING of FCC  FINAL TEXTURE
The superimposed shear breaks the orthotropic symmetry of the rolling texture

## Slide 38: EXAMPLE 2: ROLLING of FCC  CHARACTERIZATION
The superimposed shear alters the final texture. As a consequence,
the yield locus,
the in-plane anisotropy (Lankford),
the directional Young modulus,
the final rolling components,
are different.
Plane strain
Plane strain + shear

## Slide 39: EXAMPLE 5: TORSION of FCC  fixed ends
Simulate torsion (simple shear) of an initially random FCC aggregate.
Deformation by slip in the <110> direction and on {111} crystallographic planes, up to e12 = 2.0
The Voce hardening is linearly increasing:
Case 5a: the imposed velocity gradient is fixed-end mode
the hoop and radial stress components are imposed to zero
2
3
1

## Slide 40: EXAMPLE 5: TORSION of FCC  process sequence
The sequence of processes enforced through VPSC7.IN are:
1- 40 steps of
2- calculation of intermediate yield surface, projection
3- 40 steps of
4- calculation of the final yield surface, projection
*NUMBER OF PROCESSES
4
*IVGVAR AND PATH\NAME OF FILE; STRESS SUBSP OR ANG INCR
0
example5\torsion.a
2 ivgvar=2 will calculate PCYS at the end
1 5 --> section of stress space
0
example5\torsion.a
2 ivgvar=2 will calculate PCYS at the end
1 5 --> section of stress space

## Slide 41: EXAMPLE 5: TORSION of FCC  free ends
Simulate torsion (simple shear) of an initially random FCC aggregate.
Deformation by slip in the <110> direction and on {111} crystallographic planes, up to
The Voce hardening is linearly increasing:
Case 5b: the imposed velocity gradient is free-end mode
the hoop and radial stress components are imposed as zero
2
3
1

## Slide 42: EXAMPLE 5: TORSION of FCC  FINAL TEXTURE
Textures are typical of shear.
A slight rotation of the texture between fix-end and free-end is responsible for the rotation of the yield locus and the associated change in length.

## Slide 43: EXAMPLE 5: TORSION of FCC  CHARACTERIZATION
FIXED END:
Axial strain is zero  strain rate perpendicular to the yield surface AND vertical.
Fixed-end torsion
Free-end torsion
FREE END:
Axial stress is zero  strain rate perpendicular to the yield surface AND stress vector vertical.

## Slide 44: Plotting Results from VPSC: packages and installation
Suggestion: use MTEX, which is available as an open source package within MATLAB. MATLAB is freely available for academic use for members of CMU.
Step 1: install MATLAB
Step 2: search on “github mtex” to find the webpage. Download it as a zip file. Unpack the zip.
Step 3: open MATLAB and add the path to the MTEX folder.

## Slide 45: Plotting Results : Using MTEX
Step 1: edit the file TEX_PH1-compression1.OUT, where the name depends on what you have in the VPSC control file, vpsc7.in. You can always do this by hand but a python/bash script would be worth implementing to automate it.
  Each texture output has 4 header lines. Insert “#” at the beginning of each of those lines. Add a 5th line that reads “ phi1 Phi phi2 weight” so that MTEX can read in appropriate headers for each of the 4 columns of data.
Go to https://mtex-toolbox.github.io/OrientationImport.html to find an example of how to import lists of orientations.
  For fcc metals such as Al, use cs = crystalSymmetry.load(‘Al-Aluminum.cif’) to load the correct crystal symmetry
  Add Folder to the MATLAB path where you have the VPSC results (with the edited TEX list).
  fname = fullfile(‘~/code/CarlosTome-self-consistent/vpsc7d_noexe/Al_Rollett ','TEX_PH1-compression1-headers.txt’); note the different path name to the data
  plotPDF(ori,Miller({1,1,1},{0,0,1},{1,0,1},cs)); note the different set of Miller indices to specify which poles to plot

## Slide 46: Plotting Results: MTEX, odf
https://mtex-toolbox.github.io/ODFTutorial.html
This command should work to compute the odf from the list of orientations: odf = calcDensity(ori)
Assuming that you succeed in computing the odf, many different kinds of plot are possible.
See https://mtex-toolbox.github.io/orientation.calcDensity.html for more detail of options (kernel width, e.g.)
pf = calcPoleFigure(odf,Miller({1,1,1},{0,0,1},{1,0,1},cs))

## Slide 47: Pole Figures
https://mtex-toolbox.github.io/PoleFigure.plot.html
plot(pf,'contourf')